# METAL	BAR GRATING

## AMERICAN NATIONAL STANDARD

ANSSTANI/NAADARDMM          MBG 531-24

GRA TINGS

5

ANS I/NAAM M — B-531

July 15, 2024

METAL BAR GRATING

MANUAL

NINTH EDITION

• Maximum Bearing Bar Depth  .  .  .  . 21/2 ” (63 .5 mm)

• Maximum Bearing Bar Thickness

Steel & Stainless Steel  .  .  .  .  .  .  .  .  . 3/16 ” (4 .8 mm)

Aluminum  .   .   .   .   .   .   .   .  .  .  .  .  .  .  .  .  .  .  .   1/4 ” (6 .4 mm)

• Maximum Depth of I-Bar  .  .  .  .  .  .  .  . 21/2 ” (63 .5 mm)

ANS I/NAAM M — M  G 531-4

July 15, 2024

5

GRA TINGS

derian Nati。naist

A Division of

NATIONAL ASSOCIATION OF

ARCHITECTURAL METAL MANUFACTURERS

ANSI/NAAMM MBG 531-24

National Association of Architectural Metal Manufacturers

800 Roosevelt Road

Bldg. C, Suite 312

Glen Ellyn, Illinois 60137

Phone: (630) 942-6591 Fax: (630) 790-3095

www.naamm.org

Copyright © 1967, 1974, 1979, 1988, 1994 (Reprinted 1997), 2001, 2009,

2017, 2024 National Association of Architectural Metal Manufacturers

All Rights Reserved

ANSI/NAAMM MBG 531-24

Ninth Edition

NAAMM MBG 531

800 Roosevelt Road

Bldg. C, Suite 312

Glen Ellyn, Illinois 60137

Phone: (630) 942-6591

www.naamm.org

email: info@naamm.org

NAAMMS METAL BAR GRATING DIVISION

The  members  of  the  Metal  Bar  Grating  Division  of  the  National Association of Architectural Metal Manufacturers have supported the preparation  of  this  Manual.  All  are  producers  and/or  suppliers  of products conforming to the standards and specifications   contained herein. A copy of the Membership Roster of the Metal Bar Grating Division is available from NAAMM at www.naamm.org.

ANSI/NAAMM MBG 531-24

FOREWORD

The  NAAMM  Metal  Bar  Grating   Manual  provides  architects  and  engineers with  current technical data on bar gratings and stair treads of steel, stainless steel,   and   aluminum.    The   information   contained    is    based    on   sound engineering   principles   and    reflects   practices    recommended    by   leading manufacturers in the industry.

The  first  eight  editions  of  the  manual  have  been  widely  used  by  the

design professions.  In  preparing  this  ninth  edition,  the  Metal  Bar  Grating Division  of  NAAMM  has  reviewed its contents in detail and has made

revisions to reflect current practices.

The  load  tables  in  this  edition  are  based  on  the  design  formulas  and procedures found in ANSI/NAAMM MBG 534-14 Metal Bar Grating Engineering Design Manual, which was developed to provide a clearer understanding of the procedures used in the design of grating and treads.

Also  included  are  metric  equivalents  as  an  aid  to  designers  who  use  the metric system.  The  system  of   metric   measurement   used   is  from   IEEE/ ASTM  SI  10-2010, “Standard for Use of the International System of Units (SI): The Modern Metric System”.

The stair treads shown in this standard have been tested and conform to the requirements of OSHA 29CFR 1910.24(c), IBC 2012.

Changes from the previous edition, ANSI/NAAMM MBG 531-17 are indicated by the placement of a vertical line next to the changed item. It should also be noted that the Code of Standard Practice has been removed.

Standard Marking System  	4

Standard Gratings   	6

Minimum Sizes and Tolerances of Bars    	7

Load Tables / Inch-Pound units

Steel  	8

Stainless Steel   	10

Aluminum   	12

Load Tables / Sl units

Steel  	9

Stainless Steel   	11

Aluminum   	13

Anchoring Details	14

Installation Notes; Panel Dimensions 	15

Installation Clearances 	16

Operation and Maintenance Instructions  	17

Standard Tread Nosings   	18

Tread Dimensions and Details 	19

Manufacturing Tolerances  	20

Welding Standards  	21

Grating Uses  	22

Information to be Provided when Ordering	23

Standard Specifications  	24

Glossary of Terms  	25

Bearing bar spacing is designated by a number which indicates sixteenths of an inch, or mm.

For  welded   or  pressure-locked  grating  this   is  the distance, in sixteenths of an inch, or mm, center-to- center of bars.

For riveted grating it is the distance, in sixteenths of an inch, or mm, between bearing bar faces.

Cross bar or rivet spacing is designated by a number which indicates inches, or mm.

For  welded   or  pressure-locked  grating  this   is  the distance, in inches, or mm, center-to-center of cross bars. For riveted grating it is the distance in inches, or mm, center-to-center of rivets, measured along a single bearing bar.

The size  of  bearing  bars  is  expressed  in  inches  of depth and thicknesses as follows:

*Equivalent bearing bar sizes in millimeters

are obtained by a multiplication factor of 25.4

TYPE

| W-19-4 (1 x 3/16) steel W-30-102 (25 x 4.8) |  |
| --- | --- |
|  | (25 mm x 4.8 mm) |
| R-18-7 (11/4 x 1/8) stainless steel R-29-178 (32 x 3.2) |  |
|  | (32 mm x 3.2 mm) |
| P-15-2 (11/4 x 3/16) aluminum P-24-51 (32 x 4.8) |  |
|  | (32 mm x 4.8 mm) |
| P-19-4 (11/2 I Bar) aluminum P-30-102 (38 I Bar) |  |
|  | (38 mm I Bar) |

Type W-19-4 (W-30-102)

Type P-19-4 (P-30-102)

# RIVETED*

Type R-18-7 (R-29-178)

Riveted   grating   is   also available  with  a  double crimp in the reticuline bar:

STEEL / STAINLESS STEEL                                WELDED*

| Bearing Bars |  | Minimum Cross Bar Size |  |
| --- | --- | --- | --- |
| Thickness in. (mm) | Depth in. (mm) | Section Area in.2 (mm2) | Weight lb/ft (kg/m) |
| 1/8 (3.2) 1/8 (3.2) 3/16 (4.8) 3/16 (4.8) | 3/4 (19) thru 1 (25) 11/4 (32) thru 11/2 (38) 3/4 (19) thru 11/2 (38) 13/4 (44) thru 21/2 (64) | .031 (20) .049 (32) .049 (32) .062 (40) | .107 (.159) .167 (.248) .167 (.248) .211 (.314) |

*Minimum size shown is for cross bars on 4 inch centers. When cross  bars  are  on  2  inch  centers,  the  minimum  size  may  be reduced by 25%.

STEEL / STAINLESS STEEL / ALUMINUM                                                                                        PRESSURE - LOCKED

Cross bars are made in a variety of solid and hollow shapes. They can be of any size and configuration which will provide structural stability under the stated design loads.

STEEL / STAINLESS STEEL                                  RIVETED

| Bearing Bar Depth in. (mm) | Minimum Size of Connecting (Reticuline) Bars |  |
| --- | --- | --- |
|  | Thickness in. (mm) | Depth in. (mm) |
| 1 (25) 11/4 (32) thru 13/4 (44) 2 (51) thru 21/2 (64) | 1/8 (3.2) 1/8 (3.2) 1/8 (3.2) | 5/8 (16) 3/4 (19) 1 (25) |

| Bearing Bar Depth in. (mm) | Minimum Size of Connecting (Reticuline) Bars |  |
| --- | --- | --- |
|  | Thickness in. (mm) | Depth in. (mm) |
| 3/4 (19) 1 (25) thru 13/4 (44) 2 (51) thru 21/2 (64) | 1/8 (3.2) 1/8 (3.2) 1/8 (3.2) | 5/8 (16) 3/4 (19) 1 (25) |

ALUMINUM                                                       RIVETED

NOTE: The  following  references  were  used  as  a  guide  in  establishing  the  above bearing  bar tolerances: ASTM A  1011A (1011M) Commercial Steel Type  B, ASTM A 510 (A510M); ASTM B 221 (B221M), ASTM B 210 (B210M); Aluminum Association standards and data (extruded shapes) .

# LOAD TABLE FOR STEEL GRATING - TYPE W-19 OR P-19

See Appendix A for a graphic depicting table loading

ASTM A 1011 CS TYPE B

F=18,000psi,    E=29,000,000psi

Loads above DO NOT include the dead load of the grating .

# LOAD TABLE FOR STEEL GRATING - TYPE W-19 OR P-19

See Appendix A for a graphic depicting table loading

ASTM A 1011 CS TYPE B F=124MPa,    E=200,000MPa

Recommended max. span for 6.4mm  deflected under uniform load of 4.8kPa

Kg/m2**

Loads above DO NOT include the dead load of the grating .

## LOAD TABLE FOR STAINLESS STEEL GRATING - TYPE W-19 OR P-19

See Appendix A for a graphic depicting table loading

ALLOYS 304, 316 & 304L, 316L F=20,000psi,    E=28,000,000psi

Loads

above DO NOT include the dead load of the grating .

10

## LOAD TABLE FOR STAINLESS STEEL GRATING - TYPE W-19 OR P-19

See Appendix A for a graphic depicting table loading

ALLOYS 304, 316 & 304L, 316L F=138MPa,    E=139,000MPa

Recommended max. span for 6.4mm  deflected under uniform load of 4.8kPa

Kg/m2**

Loads above DO NOT include the dead

load of the grating .

11

## LOAD TABLE FOR ALUMINUM GRATING - TYPE P-19

See Appendix A for a graphic depicting table loading

F=12,000psi,    E=10,000,000psi

Loads above

12

DO NOT include the dead load of the grating .

## LOAD TABLE FOR ALUMINUM GRATING - TYPE P-19

See Appendix A for a graphic depicting table loading

F=83MPa,    E=69,000MPa

Recommended max. span (mm) for 6.4mm deflection under uniform load of 4.8kPa

Kg/m2**

Loads above DO NOT include the

dead load of the grating .                                                                                                    13

# GENERAL  REQUIREMENTS  FOR  GRATING  INSTALLATION

1.  Unpack grating and inspect for damage.

2.  Grating shall be installed with cross bars on top.

3.  Preliminarily install all grating into area per layout drawing.

4.  Adjust spacing between panels to allow for proper pack out and equal spacing between panels and between supports.

5.  Verify that all grating is adequately supported. Notching bearing bars at

supports or interrupting bearing bars with cutouts shall only occur when the system has been designed for such modification and is specified by the

design engineer and indicated on the plans.

6.  Securely fasten all grating as specified for project or per NAAMM

recommendations.

15

Shallow banding bar shall be 1/4 in. (6.4 mm) to 1/2 in. (13 mm) less than depth of grating to permit drainage.

Metal shall be used for all grating supports and provide a 1 in. (25 mm) minimum bearing surface for depths up to 21/4  in. (57 mm), and 2 in. (51 mm) minimum bearing surface for depth 21/2  in. (64 mm) and over, at each end of span.

1/4” (6) nominal

clearance between ends of cross bars on rectangular

grating or rivet  heads on riveted grating.

Clearances shown are recommended, but vary in accordance with dimensional tolerances shown on page 20.

Cutouts for circular obstructions are recommended to be at least 2 in. (51 mm) larger in diameter than the obstruction. It is further recommended that cutouts for all piping 4 in. (102 mm) or less in diameter be made in the field.

As shown in the drawing below, all rec- tangular  cutouts  are  made  to  the  next bearing bar beyond the penetration with

a clearance  not  to  exceed  bearing  bar spacing.

# OPERATION  AND  MAINTENANCE  INSTRUCTIONS

1.  For pedestrian load rated grating design, grating is intended for

normal walking pedestrian traffic. Precautions shall be taken to

prevent wheel or other loads beyond the design load rating for the application.

2.  For other uniform or concentrated load rating applications,

precautions shall be taken to prevent loads beyond the design load rating for the application.

3.  Periodically inspect grating for damage or excessive wear, such as corrosion, damage to the finish, deformation and excessive bearing bar lean beyond the tolerances as noted on page 20.

Repair or replace any areas showing damage.

4.  Periodically inspect grating to be sure that all grating is securely

fastened as specified for the application or as noted on page 14, if fastening method is not specified. Replace any missing attachment hardware and tighten any loose connections.

18

carrier plate

thickness  1/8” (3 mm) minimum

DIMENSION B & C in TREAD with carrier plate detail in. (mm)

| Grating Depth | # Dimension B | Dimension C |
| --- | --- | --- |
| 3/4 (19) to 11/4 (32) 11/2 (38) to 13/4 (44) | 13/4 (44) 21/4 (57) | 21/2 (63) 3 (76) |
| For aluminum and all treads over 13/4 (44) consult with manufacturer. |  |  |

# The welding standards shown here apply to those gratings and treads having

a clear opening of not less than 5⁄8  in. (16 mm) between bearing bars and those galvanized as per Specifications, page 24. See NAAMM STANDARD MBG 533 “Welding Specifications for Fabrication of Steel, Aluminum and Stainless Steel Bar Grating” for welding specifications and certification of welders.

STANDARD STAIR TREADS

( bearing bar thickness less than 1/4”(6.4mm) and bearing bar clear opening greater than or equal to 5/8” (16mm) )

5,,

(127)

5,,

(127)

1/8”(3.2)

carrier plate

1/8”(3.2)         1” (25) at mid-span*

for stair treads

3, - 0 and greater

(914mm)

1/8”(3.2)        1” (25) at mid-span*

for stair treads

3, - 0 and greater

(914mm)

carrier angle

1/8”(3.2)

when carrier plates and carrier angles are used, the bearing bars in the front five inches,

the back bearing bar, and the nosing shall be welded to the carrier plate or carrier angle as shown.

On treads over 9-3/4 in. (248) wide weld end of center bar also.

* Treads spanning 4 ft. (1.2m) or more shall have welds located at the third points.

# Type of nosing:  (see page 18 of this Manual)

20

21

e) Finishes: Carbon steel gratings shall be specified unfinished,  galvanized,  or  painted  one  coat  of manufacturer’s standard paint applied in accordance with the manufacturer’s standard practice. One coat of manufacturer’s standard paint is designed as an economical solution for many applications. Gratings specified to be galvanized shall have their exposed surfaces  zinc-coated  by  the  hot  dip  process  per ASTM A 123 after fabrication. Gratings and/or treads stored at the jobsite shall be covered or under roof.

Required covering is not the responsibility of the grating and/or tread supplier .

Unless  otherwise  specified,  abrasive  nosings  will have the manufacturer’s standard finish.

Aluminum and stainless steel gratings shall have a mill (as fabricated) finish, unless otherwise specified.

III . MATERIALS

a) Steel gratings:

Steel used in bearing bars, cross bars and connecting bars of  rectangular  section  shall  have  mechanical properties equal to, or greater than the performance of ASTM A 1011/A 1011M Commercial Steel (Type B) for hot rolled carbon steel sheet and strip. Cross bars  made  of  wire  rod  shall  conform  to  ASTM  A 510/A 510M for carbon steel wire rods and coarse round  wire,  except  that  permissible  tolerance  on diameter  of  coarse  round  wire  shall  be  ±  0.005 in. (± 0.13 mm). Combinations of these steels are permitted to be welded together.

Rivets shall be of steel prescribed in ASTM A 575, 1/4 in. (6.4 mm) minimum diameter, flat head type.

b) Aluminum gratings:

Bearing bars shall be either alloy 6005A-T61, 6061-T6, 6105-T5, or alloy 6063-T6, conforming to ASTM B 221 (B 221M). Cross bars and bent connecting bars shall be of alloy 6061 or 6063 conforming to ASTM B 221 (B 221M), or alloy 3003 conforming to ASTM B 210 (B 210M).

Rivets shall be made of aluminum wire of alloy 6053- T61 conforming to ASTM B 316/B 316M.

c) Stainless steel gratings:

Bearing bars, cross bars, and connecting bars shall

be Type 304, 304L, 316, or 316L alloy conforming to 24                      ASTM A 666.

# LOAD-CARRYING BAND

METRIC — The system of  metric measurement used is  from  IEEE/ASTM  SI   10-2010,  “Standard  for Use of the International System of Units (SI): The Modern Metric System”.

angular angular

25

26

ANSI/NAAMM MBG 531-24

APPENDIX A

Graphic Depicting the Loadings in Tables

Concentrated Mid Span Load per foot of width

Uniform Load per square foot

27