# Access

Systems

# Quick Flooring Guide

Choosing the right flooring

Load 5kPa/Deflection 5mm

## Load 2.5kPa/Deflection 5mm

| Span mm | Steel | Aluminium | FRP |
| --- | --- | --- | --- |
| 600 | C205MP | A253AP | G256 |
| 900 | C205MP | A253AP | G386 |
| 1200 | C255MP | A325AP |  |
| 1500 | A325MP | A503AP |  |
| 1800 | A405MP | A503AP |  |
| 2100 | A505MP |  |  |

Light occasional use. No public access - AS/NZS1657

### Heavy use. Occasional placement of heavy tools - AS/NZS1170

| Span mm | Steel | Aluminium | FRP |
| --- | --- | --- | --- |
| 600 | C205MP | A253AP | G256 |
| 900 | C205MP | A253AP | G386 |
| 1200 | C205MP | A255AP | G386 |
| 1500 | A255MP | A403AP |  |
| 1800 | A325MP | A503AP |  |
| 2100 | A405MP |  |  |

Load 5kPa/Deflection 10mm

| Span mm | Steel | Aluminium | FRP |
| --- | --- | --- | --- |
| 600 | C205MP | A253AP | G256 |
| 900 | C205MP | A253AP | G386 |
| 1200 | C205MP | A255AP | G386 |
| 1500 | A255MP | A403AP |  |
| 1800 | A325MP | A503AP |  |
| 2100 | C405MP |  |  |

Heavy use - Occasional placement of heavy tools - AS/NZS1170

Load 3kPa/Deflection 5mm

Light occasional use. No public access - AS/NZS1170

| Span mm | Steel | Aluminium | FRP |
| --- | --- | --- | --- |
| 600 | C205MP | A253AP | G256 |
| 900 | C205MP | A253AP | G386 |
| 1200 | C205MP | A255AP |  |
| 1500 | A255MP | A405AP |  |
| 1800 | A325MP | A505AP |  |
| 2100 | A405MP |  |  |

Load 4kPa/Deflection 5mm

Load 7.5kPa/Deflection 10mm

Span mm Steel Aluminium FRP

A205MP A205MP A205MP C325MP A405MP C505MP

600

900

1200

1500

1800

2100

A253AP

A255AP

A325AP

A405AP

A505AP

G256

G386

Heavy frequent use. No public access - AS/NZS1170

### Heavy use. Frequent placement of heavy tools - AS/NZS1170

| Span mm | Steel | Aluminium | FRP |
| --- | --- | --- | --- |
| 600 | C205MP | A253AP | G256 |
| 900 | C205MP | A255AP | G386 |
| 1200 | F255MP | A325AP |  |
| 1500 | F325MP | A405AP |  |
| 1800 | C405MP | A505AP |  |
| 2100 | C505MP |  |  |

Note kPA: (Kilopascals): Expression of Uniformly Distributed Load.

Other combinations of pattern and load bar are available beyond those listed above. See load tables on page 6/7 for more detail.

2

# Grating Patterns

STEEL

ALUMINIUM

※ stoi∩less steel potteΓ∩s oΓe the some os obove. lmoges show Mild steel.

potteΓ∩ F: show∩ i∩ seΓΓoted pΓofile.

※ FoΓ Co∩fiΓmotio∩ of stoCk po∩el widths o∩d lood boΓ multiples/ ΓefeΓ to the  webfoΓge website.

3

### Grating

Treatment/Colour: (Conditions apply)

Mild Steel Grating

•     Galvanised (G) (AS/NZS 4680)

•     Untreated (U)

Materials:

Mild Steel (M):

Recommended for high impact, high load applications where economy

and strength are paramount.

Stainless Steel Grating

•     Mill Finish (M)

•      Electropolished (E)

•      Passivated (P)

Aluminium Grating

•     Anodised (A)

•      Powder Coated (PC)

•      Painted (P)

•     Mill finish (M)

* For FRP Grating info refer to p8.

## Grating  Code Example

Grating is manufactured from a minimum of Grade 250 Mild Steel (or equivalent).

Aluminium (A):

Recommended where light weight is important and where quality of appearance is paramount. Material 6063-T6

Stainless Steel (S):

Recommended where rust resistance or hygienic environment is required. ASTM A240 GR316.

Top Surface:

## Aluminum

Standard grating comprises Plain (P) square edge flat bars. To increase  the slip resistance, Serrated (S) grating can be specified. Stainless Steel, 6mm bars, and any load bars 20mm deep will not be serrated.

P

A

A  325                  M    12

In addition, both steel and aluminium grating can improve their slip

Panel

Size    Nominal Panel sizes

12 = 1000 x 5800

resistance by setting the load bars parallel to the walking direction over the floor. In steel grating better slip resistance is available in patterns  with 100mm cross rod centres, ie Patterns A & C.

Treatment/Colour     M = Mill Finish

A = Anodised

PC = Powder Coated

As mandated by AS/NZS1657, the use of 10 x 10mm square bar cleats must be used for additional security on slopes >10.

ISO14122.1 recommends cleats between 10° and 20° .

Top

Surface     P = Plain

S = Serrated

(not avail. for load bars 20mm deep or 6mm thick)

Material

A = Aluminium (6063-T6)

Bar Size   325

255

etc

Pattern   A

B

etc.

Steel Grating  Code Example

Stainless Steel Grating   Code Example

305

A  325   M     P     G     12

A              S      P      E      9

Nominal Panel sizes

Nominal Panel sizes

9 = 1000 x 4000

6 = 1200 x 4000

E = Electropolished

M = Mill Finish P = Passivated

Panel Size

Panel Size     12 = 1000 x 5800

13 = 1200 x 5800 (Sourced from WA)

Treatment/Colour

Treatment/Colour     G = Galvanised

U = Untreated

B = Bitumen Dipped

Top Surface

P = Plain

Top Surface     P = Plain

S = Serrated

(not avail. for load bars 20mm deep or 6mm thick)

Material    S = 316 Stainless Steel

S1 = 304 Stainless Steel

Material     M = Mild Steel

Bar Size

305

255 etc

Bar Size   325

255

Pattern   A

B

etc.

etc

Pattern   A

B

etc.

4

Standard Panel Sizes: Mild Steel Grating

The standard range of panel sizes are;

Considerations when choosing Stock Panels

•       Utilise the Quick Flooring Guide to choose the most appropriate

combination of Pattern and Load Bar, for your application.

•       Add codes for options; Material, Top Surface, Treatment/Colour

•       Select a standard panel size or provide details of custom sizes (see below)

#### Considerations when choosing Custom Panels

•       Utilise the Quick Flooring Guide to choose the most appropriate combination of Pattern and Load Bar, for your application.

•       Add codes for options; Material, Top Surface, Treatment/Colour

•       Do you need panels to be ‘Banded’ or ‘Cut to Size’ only.

Code        Panel Sizes nominal

12            1000 x 5800 span

13             1200 x 5800 span *sourced from WA

Panels can be cut and fabricated to order.

Aluminium Grating

The standard range of Aluminium panel size: Code        Panel Sizes nominal

12            1000 x 5800 span

6m panels available on request.

Custom panels can be manufactured in load bar multiples up to 1200mm wide.

See website for terminology

•      Panel sizes are specified in Width & Span

(Span is always the last dimension)

Stainless Steel Grating

As dictated by the availability of raw material flat bar, usually 4000mm span. Please enquire at branch.

•       Webforge will supply panels optimised to the maximum length unless notified otherwise.

•       As standard, Webforge wont match cross rods.

*NB. Panel widths should be in load bar multiples.

See p15 for details

#### Considerations for large projects or floor areas

•       Webforge can provide a detailed quotation for large areas, based on detailed drawings of the area, including;

•  Dimensions

•  Span

•  Section size, location of and toe direction of the support steel

•  Location and size of cut outs and removable areas

•  Location of kick plate and nosings

•  Indicate if penetrations are required to be split

Panel sizes are nominal. Dimensions will vary slightly according to load bar thickness and the pattern.

### Span Direction

•       The direction that the load bars run, is known as the Span, and is important when considering supporting the grating.

•       Span is always the last dimension given when referencing a panel size

•       Grating has to be supported 90° to the span direction and does not require support on the other sides.

### Load Bar Direction

The load bar is the flat bar from which the grating is made and the support of the support of the grating has to be perpendicular to this direction. The direction of the load bar defines the span of the grating.

##### CORRECT                                             INCORRECT

5

### Steel Load Table

LOADBAR SPACING MM

4KPA5MM DEFI SPAN

LOAD BAR SIZE MM

MASS KG/M2

PRODUCT

450         600        750         900       1050      1200       1350      1500     1800      2100       2400      2700       3000     3300      3600

7.1

9.4

10.4

9.4

9.7

7.5

11.0

7.5

14.1

9.4

12.8

6.6

13.2

7.5

16.2

7.5

17.4

6.6

15.0

5.3

15.9

5.9

22.0

7.5

18.1

5.9

21.7

5.9

22.0

5.3

26.6

5.9

30.0

5.3

24.9

4.7

28.2

4.7

36.1

5.9

33.9

4.7

41.5

4.7

56.4

4.7

52.5

4.2

71.4

4.2

64.9

3.8

88.2

3.8 149.1	2.9 238.1 2.5

1000

1120

1170

1180

1190

1250

1250

1320

1320

1330

1360

1400

1410

1410

1420

1500

1540

1580

1580

1620

1650

1670

1680

1680

1760

1860

1980

1980

2030

2160

2190

2330

2800

3200

4.3

15.5

6.3

15.5

5.9

12.4

6.7

12.4

8.5

15.5

7.7

11.0

8.0

12.4

9.8

12.4

10.5

11.0

9.1

8.8

9.6

9.7

13.3

12.4

10.9

9.7

13.1

9.7

13.3

8.8

16.1

9.7

18.1

8.8

15.1

7.8

17.1

7.8

21.9

9.7

20.5

7.8

25.1

7.8

34.1

7.8

31.8

6.9

43.2

6.9

39.2

6.2

53.4

6.2

90.2

4.8 144.1 4.1

5.4

12.3

7.9

12.3

7.4

9.8

8.4

9.8

10.8

12.3

9.8

8.7

10.1

9.8

12.4

9.8

13.3

8.7

11.5

6.9

12.2

7.7

16.9

9.8

13.8

7.7

16.6

7.7

16.9

6.9

20.3

7.7

23.0

6.9

19.1

6.1

21.6

6.1

27.7

7.7

25.9

6.1

31.8

6.1

43.2

6.1

40.2

5.4

54.7

5.4

49.7

4.9

67.5

4.9 114.1	3.8 182.3 3.3

3.5

19.2

5.1

19.2

4.8

15.3

5.4

15.3

6.9

19.2

6.3

13.6

6.5

15.3

7.9

15.3

8.5

13.6

7.3

10.8

7.8

12.0

10.8

15.3

8.9

12.0

10.6

12.0

10.8

10.8

13.0

12.0

14.7

10.8

12.2

9.6

13.8

9.6

17.7

12.0

16.6

9.6

20.3

9.6

27.7

9.6

25.7

8.5

35.0

8.5

31.8

7.7

43.2

7.7

73.0

5.9 116.7 5.1

2.4

27.6

3.5

27.6

3.3

22.1

3.8

22.1

4.8

27.6

4.4

19.5

4.5

22.1

5.5

22.1

5.9

19.5

5.1

15.6

5.4

17.2

7.5

22.1

6.1

17.2

7.4

17.2

7.5

15.6

9.0

17.2

10.2

15.6

8.5

13.8

9.6

13.8

12.3

17.2

11.5

13.8

14.1

13.8

19.2

13.8

17.9

12.3

24.3

12.3

22.1

11.0

30.0

11.0

50.7

8.5

81.0

7.4

60

40

40

40

60

30

40

30

30

40

40

30

60

40

30

30

60

30

40

40

40

30

40

60

30

30

30

40

30

30

40

30

40

30

30

30

9.6

6.9

14.1

6.9

13.2

5.5

15.0

5.5

19.2

6.9

17.4

4.9

18.0

5.5

22.1

5.5

23.7

4.9

20.4

3.9

21.7

4.3

30.0

5.5

24.6

4.3

29.5

4.3

30.0

3.9

36.2

4.3

40.8

3.9

33.9

3.4

38.4

3.4

49.2

4.3

46.1

3.4

56.5

3.4

76.8

3.4

71.5

3.1

97.2

3.1

88.3

2.8 120.0	2.8 202.9	2.1 324.1 1.8

21.6

3.1

31.8

3.1

29.8

2.5

33.8

2.5

43.2

3.1

39.2

2.2

40.5

2.5

49.7

2.5

53.3

2.2

45.9

1.7

48.8

1.9

67.5

2.5

55.3

1.9

66.4

1.9

67.5

1.7

81.4

1.9

91.8

1.7

76.3

1.5

86.4

1.5 110.6		1.9 103.7		1.5 127.1		1.5 172.9		1.5 160.9		1.4 218.8		1.4 198.6		1.2 270.1		1.2 456.5	0.9 729.3 0.8

38.4

1.7

56.5

1.7

53.0

1.4

60.0

1.4

76.8

1.7

69.7

1.2

72.0

1.4

88.3

1.4

94.8

1.2

81.6

1.0

86.8

1.1 120.0 1.4

98.3

1.1 118.0		1.1 120.0		1.0 144.6		1.1 163.3		1.0 135.6	0.9 153.7	0.9 196.7		1.1 184.4	0.9 226.0	0.9 307.3	0.9 286.0	0.8 389.0	0.8 353.1	0.7 480.2	0.7 811.5	0.5 1296.5 0.5

13.8

4.8

20.3

4.8

19.1

3.8

21.6

3.8

27.7

4.8

25.1

3.4

25.9

3.8

31.8

3.8

34.1

3.4

29.4

2.7

31.2

3.0

43.2

3.8

35.4

3.0

42.5

3.0

43.2

2.7

52.1

3.0

58.8

2.7

48.8

2.4

55.3

2.4

70.8

3.0

66.4

2.4

81.4

2.4 110.6	2.4 103.0	2.1 140.0	2.1 127.1		1.9 172.9		1.9 292.2		1.5 466.8 1.3

19.8

23.3

18.3

21.3

23.2

29.7

27.4

23.1

26.1

28.3

31.3

35.1

27.3

22.5

36.5

39.5

28.1

28.8

34.4

35.4

38.4

44.5

27.4

33.6

45.8

48.9

35.2

43.6

56.6

59.6

48.7

63.3

53.7

70

90.2

123.6

20 X 5

20 X 5

25 X 3

25 X 3

25 X 5 20 X 5

25 X 5

25 X 3

25 X 3

25 X 5

25 X 5

25 X 5

32 X 5

32 X 3

25 X 5

25 X 5

32 X 5

32 X 3

32 X 5

32 X 5

32 X 5

32 X 5

40 X 3

40 X 5

32 X 5

32 X 5

40 X 3

40 X 5

40 X 5

40 X 5

45 X 5

45 X 5

50 X 5

50 X 5

65 X 5

75 X 6

F205MPU

C205MPU

C253MPU

D253MPU

F255MPU

A205MPU

C255MSU

A253MPU

B253MPU C255MPU

D255MPU A255MSU

F325MSU

C323MPU

A255MPU

B255MPU

F325MPU

A323MPU

C325MSU

C325MPU

D325MPU A325MSU

C403MPU

F405MPU

A325MPU

B325MPU

A403MPU

C405MPU

A405MPU

B405MPU C455MPU

A455MPU

C505MPU

A505MPU

A655MPU

A756MPU

(KPA) (MM) (KPA) (MM) (KPA) (MM) (KPA) (MM) (KPA) (MM) (KPA) (MM) (KPA) (MM) (KPA) (MM) (KPA) (MM) (KPA) (MM) (KPA) (MM) (KPA) (MM) (KPA) (MM) (KPA) (MM) (KPA) (MM) (KPA) (MM) (KPA) (MM) (KPA) (MM) (KPA) (MM) (KPA) (MM) (KPA) (MM) (KPA) (MM) (KPA) (MM) (KPA) (MM) (KPA) (MM) (KPA) (MM) (KPA) (MM) (KPA) (MM) (KPA) (MM)

U

D

U

D

U

D

U

D

U

D

U

D

U

D

U

D

U

D

U

D

U

D

U

D

U

D

U

D

U

D

U

D

U

D

U

D

U

D

U

D

U

D

U

D

U

D

U

D

U

D

U

D

U

D

U

D

U

D

2.6

37.5

2.4

30.0

2.8

30.0

3.5

37.5

3.2

26.6

3.3

30.0

4.1

30.0

4.4

26.6

3.7

21.2

4.0

23.5

5.5

30.0

4.5

23.5

5.4

23.5

5.5

21.2

6.6

23.5

7.5

21.2

6.2

18.8

7.1

18.8

9.0

23.5

8.5

18.8

10.4

18.8

14.1

18.8

13.1

16.7

17.9

16.7

16.2

15.0

22.0

15.0

37.3

11.6

59.5

10.0

2.7

49.0

2.5

34.7

2.5

39.2

3.1

39.2

3.3

34.7

2.9

27.7

3.1

30.6

4.2

39.2

3.5

30.6

4.1

30.6

4.2

27.7

5.1

30.6

5.7

27.7

4.8

24.5

5.4

24.5

6.9

30.6

6.5

24.5

7.9

24.5

10.8

24.5

10.1

21.8

13.7

21.8

12.4

19.6

16.9

19.6

28.5

15.1

45.6

13.1

2.5

49.6

2.6

43.9

2.3

35.1

2.4

38.8

3.3

49.6

2.7

38.8

3.3

38.8

3.3

35.1

4.0

38.8

4.5

35.1

3.8

31.0

4.3

31.0

5.5

38.8

5.1

31.0

6.3

31.0

8.5

31.0

7.9

27.6

10.8

27.6

9.8

24.8

13.3

24.8

22.5

19.1

36.0

16.5

2.2

47.9

2.7

47.9

2.7

43.3

3.3

47.9

3.7

43.3

3.1

38.3

3.5

38.3

4.4

47.9

4.1

38.3

5.1

38.3

6.9

38.3

6.4

34.0

8.8

34.0

7.9

30.6

10.8

30.6

18.3

23.6

29.2

20.4

4.2

46.3

5.7

46.3

5.3

41.2

7.2

41.2

6.6

37.1

8.9

37.1

15.1

28.5

24.1

24.7

3.5

55.2

4.8

55.2

4.5

49.0

6.1

49.0

5.5

44.1

7.5

44.1

12.7

33.9

20.3

29.4

SPAN MM

Spo∩s i∩ the doΓkeΓ shodi∩g (to the left of the heovy li∩e) hove o delectio∩ of less tho∩ 5mm foΓ o 4kPo u∩ifoΓmly distΓibuted lood. Moss show∩ is u∩tΓeoted o∩d u∩bo∩ded. Golvo∩isi∩g o∩d bo∩di∩g will i∩cΓeose the moss os follows; A/B PotteΓ∩ 12% ∩omi∩ol C/D PotteΓ∩ 14% ∩omi∩ol F PotteΓ∩ 16% ∩omi∩ol Lood delectio∩ tobles oΓe oΓΓo∩ged i∩ Γisi∩g stΓe∩gth oΓdeΓ. See the 4kPo, 5mm delectio∩ colum∩. U = SupeΓimposed u∩ifoΓmly distΓibuted lood i∩ kPo (100kg/m2 = 0.98kPo) D = delectio∩ i∩ mm foΓ the lood U Assumptio∩s foΓ lood copocity is o∩ si∩gle spo∩s Bosed o∩ ollowoble stΓess of 171 mPo foΓ steel. Recomme∩ded mi∩imum lo∩di∩g is equol to gΓoti∩g depth (mi∩imum 25mm).

6

# Aluminium Load Table

PRODUCT

LOAD BAR SIZE MM

LOADBAR SPACING MM

MASS KG/M2

4KPA5MM DEFI SPAN

SPAN MM

450         600        750         900       1050      1200       1350      1500     1800      2100       2400      2700       3000

97.2

77.8

2.2

97.2

2.0

77.8

2.8

77.8

4.0

72.4

4.6

77.8

4.3

62.2

5.3

62.2

9.0

47.9

3.4

19.9

5.0

19.9

5.4

17.6

6.8

19.9

8.3

19.9

8.9

17.6

8.2

15.6

11.3

19.9

8.7

12.4

11.1

15.6

13.6

15.6

15.4

14.1

12.8

12.4

18.5

15.6

17.4

12.4

21.3

12.4

25.2

11.6

20.0

10.0

29.0

12.4

27.0

11.1

27.2

10.0

36.7

11.1

33.3

10.0

45.3

10.0

56.2

7.7

2.2

31.1

3.2

31.1

3.4

27.5

4.3

31.1

5.3

31.1

5.7

27.5

5.2

24.3

7.2

31.1

5.6

19.4

7.1

24.3

8.7

24.3

9.8

22.0

8.2

19.4

11.9

24.3

11.1

19.4

13.6

19.4

16.1

18.1

12.8

15.6

18.5

19.4

17.3

17.3

17.4

15.6

23.5

17.3

21.3

15.6

29.0

15.6

36.0

12.0

1.5

44.8

2.2

44.8

2.4

39.6

3.0

44.8

3.7

44.8

4.0

39.6

3.6

35.0

5.0

44.8

3.9

28.0

4.9

35.0

6.1

35.0

6.8

31.7

5.7

28.0

8.2

35.0

7.7

28.0

9.5

28.0

11.2

26.1

8.9

22.4

12.9

28.0

12.0

24.9

12.1

22.4

16.3

24.9

14.8

22.4

20.1

22.4

25.0

17.2

F253APM

C253APM

A253ASM

A253APM

C255APM

A255ASM

C323APM

A255APM

F403APM

A323APM

C325APM

A325ASM

C403APM

A325APM

A403APM

C405APM

A405ASM

C503APM

A405APM

C455APM

A503APM

A455APM

C505APM

A505APM

C655APM

U (KPA) D (MM) U (KPA) D (MM) U (KPA) D (MM) U (KPA) D (MM) U (KPA) D (MM) U (KPA) D (MM) U (KPA) D (MM) U (KPA) D (MM) U (KPA) D (MM) U (KPA) D (MM) U (KPA) D (MM) U (KPA) D (MM) U (KPA) D (MM) U (KPA) D (MM) U (KPA) D (MM) U (KPA) D (MM) U (KPA) D (MM) U (KPA) D (MM) U (KPA) D (MM) U (KPA) D (MM) U (KPA) D (MM) U (KPA) D (MM) U (KPA) D (MM) U (KPA) D (MM) U (KPA) D (MM)

25 X 3

25 X 3

25 X 3

25 X 3

25 X 5

25 X 5

32 X 3 25 X 5

40 X 3 32 X 3 32 X 5 32 X 5

40 X 3 32 X 5

40 X 3

40 X 5

40 X 5

50 X 3 40 X 5 45 X 5

50 X 3 45 X 5

50 X 5

50 X 5

65 X 5

24.1

2.8

35.5

2.8

38.1

2.5

48.3

2.8

59.2

2.8

63.6

2.5

58.2

2.2

80.5

2.8

61.8

1.8

79.1

2.2

96.9

2.2 109.4 2.0

90.9

1.8 131.8	2.2 123.6		1.8 151.4		1.8 179.2		1.6 142.0		1.4 206.0		1.8 191.7		1.6 193.1		1.4 260.7		1.6 236.6		1.4 321.8		1.4 399.9 1.1

13.6

5.0

20.0

5.0

21.5

4.4

27.2

5.0

33.3

5.0

35.8

4.4

32.7

3.9

45.3

5.0

34.8

3.1

44.5

3.9

54.5

3.9

61.5

3.5

51.1

3.1

74.1

3.9

69.5

3.1

85.2

3.1 100.8 2.9

79.9

2.5 115.9	3.1 107.8	2.8 108.6	2.5 146.6	2.8 133.1	2.5 181.0	2.5 224.9 1.9

0.7 100.8	1.0 100.8 1.1

89.2

1.3 100.8	1.6 100.8 1.8

89.2

1.6

78.8

2.2 100.8 1.7

63.0

2.2

78.8

2.7

78.8

3.0

71.3

2.5

63.0

3.7

78.8

3.4

63.0

4.2

63.0

5.0

58.7

3.9

50.4

5.7

63.0

5.3

56.0

5.4

50.4

7.2

56.0

6.6

50.4

8.9

50.4

11.1

38.8

8.7

7.8

12.8

7.8

13.7

6.9

17.4

7.8

21.3

7.8

22.9

6.9

20.9

6.1

29.0

7.8

22.2

4.9

28.5

6.1

34.9

6.1

39.4

5.5

32.7

4.9

47.5

6.1

44.5

4.9

54.5

4.9

64.5

4.5

51.1

3.9

74.1

4.9

69.0

4.3

69.5

3.9

93.8

4.3

85.2

3.9 115.9	3.9 144.0 3.0

6.0

11.2

8.9

11.2

9.5

9.9

12.1

11.2

14.8

11.2

15.9

9.9

14.5

8.8

20.1

11.2

15.4

7.0

19.8

8.8

24.2

8.8

27.4

7.9

22.7

7.0

33.0

8.8

30.9

7.0

37.9

7.0

44.8

6.5

35.5

5.6

51.5

7.0

47.9

6.2

48.3

5.6

65.2

6.2

59.2

5.6

80.5

5.6 100.0 4.3

750

890

900

950

1010

1020

1070

1080

1130

1140

1210

1240

1260

1300

1350

1430

1480

1490

1530

1560

1600

1670

1690

1810

2050

0.8

79.7

1.2

79.7

1.3

70.5

1.7

79.7

2.1

79.7

2.2

70.5

2.0

62.2

2.8

79.7

2.2

49.8

2.8

62.2

3.4

62.2

3.8

56.3

3.2

49.8

4.6

62.2

4.3

49.8

5.3

49.8

6.3

46.3

5.0

39.8

7.2

49.8

6.7

44.3

6.8

39.8

9.2

44.3

8.3

39.8

11.3

39.8

14.1

30.6

2.7

25.2

3.9

25.2

4.2

22.3

5.4

25.2

6.6

25.2

7.1

22.3

6.5

19.7

8.9

25.2

6.9

15.8

8.8

19.7

10.8

19.7

12.2

17.8

10.1

15.8

14.6

19.7

13.7

15.8

16.8

15.8

19.9

14.7

15.8

12.6

22.9

15.8

21.3

14.0

21.5

12.6

29.0

14.0

26.3

12.6

35.8

12.6

44.4

9.7

4.4

15.2

6.5

15.2

7.0

13.5

8.9

15.2

10.9

15.2

11.7

13.5

10.7

11.9

14.8

15.2

11.3

9.5

14.5

11.9

17.8

11.9

20.1

10.8

16.7

9.5

24.2

11.9

22.7

9.5

27.8

9.5

32.9

8.9

26.1

7.6

37.8

9.5

35.2

8.5

35.5

7.6

47.9

8.5

43.5

7.6

59.1

7.6

73.5

5.9

1.1

61.0

1.6

61.0

1.8

54.0

2.2

61.0

2.7

61.0

2.9

54.0

2.7

47.6

3.7

61.0

2.8

38.1

3.6

47.6

4.5

47.6

5.0

43.1

4.2

38.1

6.1

47.6

5.7

38.1

7.0

38.1

8.2

35.5

6.5

30.5

9.5

38.1

8.8

33.9

8.9

30.5

12.0

33.9

10.9

30.5

14.8

30.5

18.4

23.5

7

7

8.4

8.7

10.5

12.8

8.4

13.3

9.2

10.6

12.9

16

10.1

16.5

12.8

15.7

19.8

12.2

20.2

17.5

15.6

22.6

19.2

24.9

24.5

60

40

30

30

40

30

40

30

60

30

40

30

40

30

30

40

30

40

30

40

30

30

40

30

40

0.5 124.5	0.8 124.5	0.9 110.1		1.1 124.5		1.3 124.5		1.4 110.1 1.3

1.8 124.5 1.4

1.8

97.2

4.3

69.1

5.9

69.1

3.0

97.2

3.2

62.2

7.2

62.2

2.5

88.0

3.4

77.8

Spo∩s i∩ the doΓkeΓ shodi∩g (to the left of the heovy li∩e) hove o delectio∩ of less tho∩ 5mm foΓ o 4kPo u∩ifoΓmly distΓibuted lood. Moss show∩ is u∩tΓeoted o∩d u∩bo∩ded. Bo∩di∩g will i∩cΓeose the moss os follows; A/B PotteΓ∩  10% ∩omi∩ol C/D PotteΓ∩  12% ∩omi∩ol F PotteΓ∩  14% ∩omi∩ol Lood delectio∩ tobles oΓe oΓΓo∩ged i∩ Γisi∩g stΓe∩gth oΓdeΓ. See the 4kPo/ 5mm delectio∩ colum∩. U = SupeΓimposed u∩ifoΓmly distΓibuted lood i∩ kPo (100kg/m2 = 0.98kPo) D = delectio∩ i∩ mm foΓ the lood U Assumptio∩s foΓ lood copocity is o∩ si∩gle spo∩s. Recomme∩ded mi∩imum lo∩di∩g is equol to gΓoti∩g depth (mi∩imum 25mm).

• Stoi∩less Steel Lood Toble ovoiloble fΓom the website.

7

### FRP Grating

| Patterns: | Features / Benefits |
| --- | --- |
| Standard Mesh |  |
|  | • Integral, one piece construction increases load-bearing capabilities • Load applied to Webforge FRP bar is transferred to adjoining bearing |

bars, assisting in load distribution on the grating as well as on the support structure.

•      Smooth resin-rich vertical surfaces and tapered bars allow all debris to fall through

•      Continuous glass fibre strand in alternating layers thoroughly wetted with the appropriate resin for excellent corrosion resistance.

Material:

##### Mini Mesh

•     Isopthalic Polyester Resin (I) ASTM E-84 Fire Rating Class A, 25 or less

•     Vinyl Ester Rein (V) ASTM E-84 Fire Rating Class A, 25 or less

Top Surface:

FRP grating is provided with an antiskid Grit (G) surface as standard.

This is a coarse grit that is embedded into the top surface of the grating. A plain top surface is available on request.

Treatment/Colour:

•     Green (G) – Isopthalic Polyester Resin or

*NB. Mini Mesh is only available in 38mm deep bars

* Aperture is 12x 12mm

•    Yellow (Y) – Vinyl Ester Resin

•     Dark Grey (D) – Mini Mesh only

•     Others colours available on request

Panel Size:

The standard range of panel size is shown below:

Code        Panel Size

1              1220 x 3660

FRP Grating

G  256    I      G     G      1

FRP Load Table

Panel Size

1 = 1220 x 3660

U (kPa)

D (mm)

Treatment/Colour

Y = Yellow

D = Dark Grey

G = Green

Top Surface

G= Grit

P = Plain

785

990

Material     I = Isopthalic Polyester

V = Vinyl Ester

1035

15             10              4        2.5        2.5 1.6         4.1        4.1        5.1       15.3

15          15            10              5           2.5 1.0         2.4        3.7        3.8        5.9

15             15            10           7.5        2.5 1.0         2.4        3.6        4.7        4.8

Bar Size   256

U = Uniformly Distributed Load in kPa D = Deflection in mm

386

38619 (refers to Minimesh)

Pattern   G = FRP

8

# FRP Grating

Webforge FRP Grating - Chemical Resistance Table

%

Concentration

Vinyl Ester

Isophthalic

CHEMICAL

ENVIRONMENT

ºC

TEMP

ENVIRONMENT        Concentration    TEMP        Ester

CHEMICAL                %            ºC           Vinyl    Isophthalic

| Acetic Acid | 25 | MAX | C | C |
| --- | --- | --- | --- | --- |
| Acetic Acid | 50 | MAX | C | C |
| Aluminum Hydroxide | ALL | MAX | C | C |
| Ammonium Chloride | ALL | 48.8 | C | C |
| Ammonium Bicarbonate | 15 | 48.8 | C | C |
| Ammonium Bicarbonate | 50 | 48.8 | C | C |
| Almmonium Hydroxide | 20 | 26.6 | S | N |
| Ammonium Sulfate | ALL | 488 | C | C |
| Benzene | 100 | 65.5 | I | I |
| Benzoic Acid (SAT) | SAT | MAX | C | C |
| Borax (SAT) | SAT | MAX | C | C |
| Calcium Carbonate | ALL | MAX | C | C |
| Calcium Nitrate | ALL | MAX | C | C |
| Carbon Tetrachloride | 100 | 26.6 | I | N |
| Chlorine, Dry Gas * | ALL | MAX | C | C |
| Chlorine Water (SAT) | SAT | 48.8 | C | I |
| Chromic Acid | 50 | 65.5 | I | N |
| Citric Acid | ALL | MAX | C | C |
| Copper Chloride | ALL | MAX | C | C |
| Copper Cyanide | ALL | 60 | C | S |
| Copper Nitrate | ALL | MAX | C | C |
| Ethanol | 10 | 488 | C | S |
| Ethanol | 50 | 488 | C | I |
| Ethylene Glycol | ALL | 65.5 | C | C |
| Ferric Chloride | 100 | MAX | C | C |
| Ferrous Chloride | ALL | MAX | C | C |
| Formaldehyde 0-50% | 50 | 48.8 | S | I |
| Gasoline | ALL | 48.8 | C | C |
| Glucose | ALL | 48.8 | C | C |
| Glycerin | 100 | MAX | C | C |
| Hydrobromic Acid | 50 | MAX | S | S |
| Hydrochloric Acid | 10 | MAX | C | S |
| Hydrochloric Acid | 37 | MAX | I | S |
| Hydrogen Peroxide | 30 | 26.6 | C | N |

Lactic Acid                  100         MAX          C           C

Lithium Chloride (SAT)      SAT           MAX         N             N

Magnesium Chloride        ALL           MAX            C             C

Magnesium Nitrate          ALL         MAX         C             C

Magnesium Sulfate           ALL           MAX            C             C

Mercuric Chloride            ALL            MAX            C             C

Mercurous Chloride           ALL            MAX           C              C

Nickel Chloride            ALL         MAX         C             C

Nickel Sulfate                ALL           MAX             C             C

Nitric Acid                   20            48.8         S             S

Oxalic Acid               ALL            65.5            C           C

Perchloric Acid               30            32.2           S             I

Phosphoric Acid               80          MAX            C             C

Potassium Chloride         ALL         MAX         C             C

Potassium Dichromate      ALL           MAX            C             C

Potassium Nitrate          ALL         MAX         C             C

Potassium Sulfate          ALL         MAX         C             C

Propylene Glycol          ALL         MAX         C             C

Sodium Acetate           ALL         MAX         C           C

Sodium Bisulfate            ALL         26.6         S             S

Sodium Bromide          ALL         26.6          C             C

Sodium Cyanide             ALL           26.6            C             I

Sodium Hydroxide            10          MAX           C             I

Sodium Hydroxide          50          MAX           S           N

Sodium Nitrate              ALL            MAX           C              C

Sodium Sulfate              ALL            MAX            C             C

Sulfuric Acid                  10            MAX            C             S

Sulfuric Acid              25          MAX         C           S

Sulfuric Acid                 75            37.7           C              I

Tartaric Acid                 ALL            MAX            C              C

Vinegar                 ALL            MAX            C              C

Water, Distilled              ALL         MAX         C             C

Zinc Nitrite               100           MAX         C             C

Zinc Sulfate                 100            MAX         C             C

C = Continuous exposure of the grating to the Chemical Environment listed at the temperature listed

S = Frequent exposure of the grating to splashes and spills the Chemical Environment listed with that environment at the temperature listed

I = Infrequent Exposure of the grating to splashes and spills from the Chemical Environment listed with that environment at the temperature listed and the spill immediately cleaned up or washed from the grating .

N = Not recommended for the concentrations and temperatures listed

T =Test

MAX = indicates temperature of 85ºC for molded VinyI Ester . 71ºC for moulded Isopthalic grating.

ALL = All concentrations SAT = Saturated solution

9

### Stair Treads

Steel

T3 – Welded Fixing, Floor plate Nosing

T5 – Welded Fixing, Abrasive Nosing

T1 – Welded Fixing, No Nosing

T4 – Bolted Fixing, Floor plate Nosing

T6 – Bolted Fixing, Abrasive Nosing

T2 – Bolted Fixing, No Nosing

### Aluminium

T3 – Welded Fixing, Floor plate Nosing

T5 – Welded Fixing, Abrasive Nosing

T1 – Welded Fixing, No Nosing

T4 – Bolted Fixing, Floor plate Nosing

T6 – Bolted Fixing, Abrasive Nosing

T2 – Bolted Fixing, No Nosing

### FRP

AS1657 requires that the nosing of the tread is clearly visible against the background.

Bolted Fixing, Abrasive Nosing

Also available in Mini Mesh.

10

### Stair Treads

The tables below indicate the maximum width and length for stair treads, depending on the

combination of material, pattern and load bar selected. Standard stair treads are available ex-stock

from Webforge locations; these standard profiles are complimented by a custom manufacturing service.

25 x 5

550

40 x 5

1600

1500

1350

40 x 5

1275

1050

700

32 x 5

1300

1200

850

25 x 6

32 x 5

900

675

450

38 x 6

25 x 5

900

750

550

-

-

-

-

-

-

-

-

875

600

-

-

-

-

-

-

Steel                                           Aluminium                                   FRP

Load Bar Size A & B Pattern C & D Pattern F Pattern

G Pattern

##### Recommended Maximum Tread Widths for Grating Patterns

Recommended Maximum Lengths for Grating Patterns

| A & B Pattern C & D Pattern F Pattern | 125 125 125 | 155 165 - | 185 - 185 | 215 205 - | 245 245 245 | 275 285 - | 305 325 305 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| G Pattern | - | - | - | - | 234 | 272 | 310 |

##### End Plates

flat bar.

The standard tread end plates for the different width stair treads are shown below.   Tread end plates are manufactured from 65 x 5 For load bars > 40mm depth, special end plates are required.

40mm minimum recommended bearing surface

125mm Tread Widths

## Standard FRP Treads

Top Saddle: C129SM

Screw: C301SM

25

4 clips per tread (angle not supplied)

## 4 clips per tread (angle not supplied)

75

Attach with:

## 215, 245, 275, 285, 305 & 325mm Tread Widths

155, 165, 185mm Tread Widths                          205,

Note: All end plates sniped at 34° unless requested otherwise

Drilling Stringers:

###### Table of recommended stair stringers drilling for M12 bolts

40mm minimum recommended bearing surface

## Minimesh Treads

Predrill angle with 7.4 Hole Attach with: Disc C140SM

4 clips per tread (angle not supplied)

Predrill angle with 7.4 Hole Attach with: Disc C140SM

Top Saddle: C129SM

Thread Rolling Screw: C309SM

Thread Rolling Screw: C309SM

4 clips per tread (angle not supplied)

Please find below a table of recommended stair stringer hole centres.

| Tread width mm Recommended stringer Hole size hole centres mm mm |  |  |
| --- | --- | --- |
| 125 | 45 | 14 dia |
| 155, 165, 185 | 75 | 14 dia |
| 205, 215 | 100 | 14 dia |
| 245, 275, 285, 305, 325 | 125 | 14 dia |

11

Mild Steel

##### Fixing Clips

CLIP SET CODE

PATTERN

COMPRISES

USAGE

Top clip C100MG Bottom C200MG

M8 x 65mm Bolt C304MG

Mild Steel Grating Depth = <50mm Flange present

Stainless Steel &  Aluminium Grating Depth = <50mm

Flange Present

C001MG

A - F

DESCRIPTION

Clip Set

Mild steel Galvanised Top, Bottom & Bolt

Aluminium

## FRP

Top Clip C100SM Bottom C200SM M8 Bolt C301SM

Top Clip C129SM M8 Bolt C301SM

C001SM

A - F

Clip Set

Stainless Steel

Top, Bottom & Bolt

FRP Grating

Depth = 25mm & 38mm

C030SM

G

Mini Mesh

Top Disc C140SM

M8 x 65mm Bolt C309SM

FRP Grating

Depth = 38mm

C033SM

Clip Set

Stainless Steel Top & Bolt

Clip Set

Mini Mesh

Stainess Steel Top & Bolt

12

# Fixing Clips

## CLIP ASSEMBLIES

Plan View

D

## TOPS

12

C140SM

Discwasher

BOTTOMS

SCREWS/RIVETS

C309SM (65 x 8)

C308MG (50 x 8)

(Pilot Hole 7.4mm)

Thread Rolling.

Web Plate

WELDING

## CLIP FREQUENCY

Nominal 4 panel, or 4 per m2, whichever is greater.

(Approximately 3 per M2 where span is >1500mm.

Fixing clips are generally not recommended in areas of vibration or where lateral or cantilever loads are applied to the grating.

13

##### Manufacturing Tolerances

width

1/100 of width

1/200 of width

1/200 of width

14

15

##### Accessories

Any steel or aluminium grating pattern can be combined with any floorplate thickness. However Webforge recommends the use of Pattern F grating. Other combinations can be supplied on request.

Webplate

Webplate is a flooring product that comprises floorplate welded to the top of the grating.

Webplate is available in the following steel or aluminium combinations

| Material | Product | Floor Treadplate Thickness | Grating | Weight Untreated Kg/sqm | Span at 4kPa UDL 5mm Deflection |
| --- | --- | --- | --- | --- | --- |
| STEEL | WP3 F255MP* | 3mm | F255MP* | 44.49 | 1390mm |
|  | WP5 F325MP* | 5mm | F325MP* | 64.78 | 1625mm |
| ALUMINIUM | WP3 F255AP* | 3mm | F255AP* | 16.21 | 1100mm |
|  | WP5 F325AP* | 5mm | F325AP* | 23.21 | 1350mm |

Where *indicates treatment, refer to the website for a detailed description of part number protocols under steel and aluminium grating sections.

WebGripTM  Anti-Slip

Available in:

• WebGripTM  Anti-Slip Stair Nosing

• WebGripTM  Metal Plating

• WebGripTM  Metal Strips

• WebGripTM  Conveyor Channel

Features:

• High Impact Resistance

• Anti-Slip Properties which overcome wet & oily surfaces

• Chermical & UV Resistance

• Durable Galvabond, Stainless Steel or Aluminium backing

• AS/NZ Certified

Stock sizes & Custom Manufactured sizes available

###### Webmesh

Webmesh comprises grating with a flattened, light gauge,

expanded mesh welded to the underside to prevent tools and small objects from falling through the grating.

Meets the requirements of AS/NZS1657 Clause 4.5 with mesh 1216F for steel grating or 1216AF for aluminium grating,

welded to the underside of the grating.

* See website for more details.

16