Grating & Related Products

1

Forging partnershipsTM

IKG is the world’s leading manufacturers of high quality steel and aluminum  bar  grating with  manufacturing  plants throughout North America.

Our skilled network of sales personnel and engineering staff is the most knowledgeable in the industry, providing consultative services  and  solutions  to  customers   in  a  wide   range  of industries.

IKG carries on the pioneering spirit of its founders, bringing experience, quality, long-term value added solutions and time- tested reliability to its customers today.

Through consistent, competitive, and dependable cutomer care, Forging Partnerships ™ has become synonymous to IKG.

# Call us at (800) 324-8417

# Advantages and Applications

When and Why to Choose Grating:

Choose grating instead of solid flooring when you need:

•     Open areas to allow passage of light, air and heat between flooring levels.

•     Flooring on which liquids and / or debris cannot collect.

•     Easy installation and fabrication.

•    Adaptability to complex floor patterns and hard-to-fit areas.

# Advantages:

# Applications:

•     High strength–to–weight ratio.

| • Strength and low weight specified • Light and air passage | • Ease of Installation • Security • Durability |
| --- | --- |

| • Industrial Flooring • Trenches • Maintenance Platforms • Walkways • Power Plants • Refineries | • Chemical Plants • Bridge Decks • Warehouses • Water and Waste Treatment Plants • Steel Mills |
| --- | --- |

All grating products are manufactured to NAAMM tolerances and specifications.

Forging partnershiSTM

Recommended for  general applications.

Same as Type W/B but with closer cross bars spacing.

Close bearing bars.

Best for heavy public

traffic, where increased carrying capacity is

required.

Same as type W/D but with closer cross bar  spacing.

4”

1- 3/16“

SPAN

2”

1- 3/16 “

SPAN

|  | 4 ” |  |
| --- | --- | --- |

15/16 “

SPAN

2”

15/16 “

SPAN

Weldforged®   Steel Grating

Forging partnershipsTM

Type

| Standard | W/B |
| --- | --- |
|  | W/F |
|  | W/D |
|  | W/DF |

| Weight lb./sf. |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Bar Size | Bearing Bar Dimensions (inches) | Grating Types |  |  |  |
|  |  | WB | WF | WD | WDF |
| 2 | 3/4” x 3/16 “ | 5.8 | 6.7 | 7.2 | 8.1 |
| 3 | 1” X 1/8” | 5.2 | 6.1 | 6.4 | 7.3 |
| 4 | 1” x 3/16” | 7.5 | 8.4 | 9.3 | 10.2 |
| 5 | 1-1/4” x 1/8” | 6.3 | 7.2 | 7.9 | 8.8 |
| 6 | 1-1/4” x 3/16” | 9.1 | 10.0 | 11.3 | 12.2 |
| 7 | 1-1/2” x 1/8” | 7.4 | 8.3 | 9.3 | 10.2 |
| 8 | 1-1/2” x 3/16” | 10.8 | 11.7 | 13.5 | 14.4 |
| 9 | 1-3/4” x 3/16” | 12.5 | 13.4 | 15.6 | 16.5 |
| 10 | 2” x 3/16” | 14.1 | 15.0 | 17.7 | 18.6 |
| 11 | 2-1/4” x 3/16” | 15.8 | 16.7 | 19.8 | 20.7 |
| 12 | 2-1/2” x 3/16” | 17.4 | 18.3 | 21.9 | 22.8 |

Twisted square cross bar*

*A round cross bar is used for Stainless Steel

Rectangular bearing bar

Forge welded joints

Surfaces:

•      Plain

•      Serrated

•      MEBAC®

Finishes:

•      Mill

•      Galvanized

•      Painted

•      GrateCoat®

Panel sizes:

•      3´ x 20´     2´ x 20´

•      3´ x 24´     2´ x 24´

Available in:

•      Carbon Steel

•      Stainless Steel (304L & 316L)

1/4” and 3/8” bearing bar thicknesses are also available. Please call for assistance.

# LOAD TABLE FOR THE WELDFORGED®  GRATING

This table is good for typeW/B and W/F only.

Forging partnershiSTM

*Recommended max. span (in.) for 1/4” deflection under uniform load of 100lb/sf.

| Size | Bearing Bar (in) | Span in inches Percentages of Open Area. Rectangular Types. Grating Type; Bearing Bar Thickness. 1/8”; 3/16”. W/B; 82.4%; 77.1%. W/F; 75.9%; 70.7%. W/D; 77.3%; 70.4%. W/DF; 70.9%; 64.1%. 237 0.372 592 0.298 658 0.134 987 0.107 196 0.451 538 0.36 121 0.730 423 0.584 140 0.629 455 0.504 1480 0.060 1480 0.048 483 0.182 846 0.146 292 0.302 658 0.241 947 0.093 1184 0.074 164 0.536 493 0.429 370 0.238 740 0.191 U D C D 67 Span in inches 96 102 101; 89; 79; 70. 0.698; 0.794; 0.897; 1.006. 379; 355; 334; 316. 0.559; 0.636; 0.718; 0.804. 90 108 * 24 U 533 D 0.099 46 C 533 D 0.079; 30 341 0.155 426 0.124; 36 237 0.223 355 0.179; 42 174 0.304 305 0.243; 48 133 0.397 266 0.318; 54 105 0.503 237 0.402; 379 0.372 158 0.372 395 0.298 334 0.451 130 0.451 359 0.360 316 0.536 110 0.536 329 0.429 Span in inches 78 93 0.629 304 0.504 84 81 0.730 282 0.584 Span in inches 60; 66; 72. 101; 84; 70. 0.466; 0.563; 0.670. 253; 230; 211. 0.372; 0.451; 0.536. 152; 125; 105. 0.466; 0.563; 0.670.. 51 U 632 D 0.074 C 632 D 0.060; 404 0.116 505 0.093; 281 0.168 421 0.134; 206 0.228 361 0.182; 158 0.298 316 0.238; 125 0.377 281 0.302. 57 U 947 D 0.074 C 947 D 0.060; 606 0.116 758 0.093; 421 0.168 632 0.134; 309 0.228 541 0.182; 237 0.298 474 0.238; 187 0.377 421 0.302. 61 U 987 D 0.06 C 987 D 0.048; 632 0.093 789 0.074; 439 0.134 658 0.107; 322 0.182 564 0.146; 247 0.238 493 0.191; 195 0.302 439 0.241. U; 1421; 909; 632; 464; 355; 281; 227; 188; 158; 135; 116. D; 0.050; 0.078; 0.112; 0.152; 0.199; 0.251; 0.310; 0.376; 0.447; 0.524; 0.608. 70. C; 1421; 1137; 947; 812; 711; 632; 568; 517; 474; 437; 406. D; 0.040; 0.062; 0.089; 0.112; 0.159; 0.201; 0.248; 0.300; 0.358; 0.420; 0.487. |
| --- | --- | --- |
| 2 | 3/4” x 3/16” |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 3 | 1” x 1/8” |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 4 | 1” x 3/16” |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 5 | 1-1/4” x 1/8” |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 6 | 1-1/4” x 3/16” |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 7 | 1-1/2” x 1/8” |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 8 | 1-1/2” x 3/16” | 77 | U D C D | 2132 0.050 2132 0.040 | 1364 0.078 1705 0.062 | 947 0.112 1421 0.089 | 696 0.152 1218 0.122 | 533 0.199 1066 0.159 | 421 0.251 947 0.201 | 341 0.310 853 0.248 | 282 0.376 775 0.300 | 237 0.447 711 0.358 | 202 0.524 656 0.420 | 174 0.608 609 0.487 | 152 0.698 568 0.559 | 133 0.794 533 0.636 | 118 0.897 502 0.718 | 105 1.006 474 0.804 |
| 9 | 1-3/4”x 3/16” | 87 | U D C D | 2901 0.043 2901 0.034 | 1857 0.067 2321 0.053 | 1289 0.096 1934 0.077 | 947 0.130 1658 0.104 | 725 0.170 1451 0.136 | 573 0.215 1289 0.172 | 464 0.266 1161 0.213 | 384 0.322 1055 0.257 | 322 0.383 967 0.306 | 275 0.450 893 0.360 | 237 0.521 829 0.417 | 206 0.599 774 0.479 | 181 0.681 725 0.545 | 161 0.769 683 0.615 | 143 0.862 645 0.689 |
| 10 | 2” x 3/16” | 96 | U D C D | 3789 0.037 3789 0.03 | 2425 0.058 3032 0.047 | 1684 0.084 2526 0.067 | 1237 0.114 2165 0.091 | 947 0.149 1895 0.119 | 749 0.189 1684 0.151 | 606 0.233 1516 0.186 | 501 0.282 1378 0.225 | 421 0.335 1263 0.268 | 359 0.393 1166 0.315 | 309 0.456 1083 0.365 | 269 0.524 1011 0.419 | 237 0.596 947 0.477 | 210 0.673 892 0.538 | 187 0.754 842 0.603 |
| 11 | 2-1/4” x 3/16” | 105 | U D C D | 4796 0.033 4796 0.026 | 3069 0.052 3837 0.041 | 2132 0.074 3197 0.06 | 1566 0.101 2741 0.081 | 1199 0.132 2398 0.106 | 947 0.168 2132 0.134 | 767 0.207 1918 0.166 | 634 0.250 1744 0.200 | 533 0.298 1599 0.238 | 454 0.350 1476 0.280 | 392 0.406 1370 0.324 | 341 0.466 1279 0.372 | 300 0.530 1199 0.424 | 266 0.598 1128 0.478 | 237 0.670 1066 0.536 |
| 12 | 2-1/2” x 3/16” | 113 | U D C D | 5921 0.03 5921 0.024 | 3789 0.047 4737 0.037 | 2632 0.067 3947 0.054 | 1933 0.091 3383 0.073 | 1480 0.119 2961 0.095 | 1170 0.151 2632 0.121 | 947 0.186 2368 0.149 | 783 0.225 2153 0.180 | 658 0.268 1974 0.215 | 561 0.315 1822 0.252 | 483 0.365 1692 0.292 | 421 0.419 1579 0.335 | 370 0.4777 1480 0.381 | 328 0.538 1393 0.431 | 292 0.603 1316 0.483 |

U = Uniform load lb./sf.                                                     C = Concentrated load lb./ft. of grating width, at mid-span.                           D = Deflection in inches.

| Type | W/D | W/DF |
| --- | --- | --- |
| Factor | 1 | .27 |

For spacings other than 1-3/16” centers, multiply the conversion factor times the U and C values shown in the table, the D (deflection) remains as shown.

| CONVERSION DATA: SERRATED GRATING |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Grating Size | 3/4” x 3/16” | 1” x 1/8” | 1” x 3/16” | 1-1/4” x 1/8” | 1-1/4” x 3/16” | 1-1/2” x 1/8” | 1-1/2” x 3/16” | 1- 3/4” x 3/16” | 2” x 3/16” | 2-1/4” x 3/16” | 2-1/2” x 3/16” |
| Multiply U & C by: | .70 | .77 | .77 | .81 | .81 | .84 | .84 | .85 | .88 | .89 | .90 |
| Multiply deflection by: | 1.20 | 1.14 | 1.14 | 1.11 | 1.11 | 1.09 | 1.09 | 1.08 | 1.07 | 1.06 | 1.05 |

Note: All deflections are theoretical and are based on standard engineering practices. They are provided for design selection only and should not be considered as absolute.

# Swage Locked Aluminum Grating

Forging partnershipsTM

Recommended for general applications.

Same as IB and BS but with closer cross bar spacing.

The close bearing bars provide a greater loading capacity than IB / BS without increasing the depth of the section.

Same as ID and DS but with closer cross bar spacing.

Our closest spaced swage lock grating. Satisfies maximum clear opening required by ADA.

With closer cross bars and bearing bars. For conditions requiring

greatly reduced net

openings. Satisfies

maximum clear opening required by ADA.

|  | 4 ” |  |
| --- | --- | --- |

1- 3/16“

SPAN

|  |  |  | 2” |  |
| --- | --- | --- | --- | --- |

1- 3/16“

SPAN

— 4 ”

15/16“

SPAN

2”

15/16“

SPAN

4”

11/16 “

SPAN

2”

11/16 “

SPAN

Type

| Standard Space | IB BS |
| --- | --- |
|  | IF FS |
| Close Space | ID DS |
|  | IDF DFS |
| Very Close Space | ICM4 SCM4 |
|  | ICMF4 SCMF4 |

Rectangular Bar Grating

(BS, FS, DS, DFS, SCM4, SCMF4)

BS swaged rectangular bar grating provides all the strength of alumi- num pressure  locked grating at a slightly lower cost. The cross bars are swaged to lock the bearing  bars in  place,  giving  you  high  strength and rigidity in a light weight, virtually maintenance free aluminum grating.

I-Bar Grating

(IB, IF, ID, IDF, ICM4, ICMF4)

Surfaces:

•      Plain

•      Serrated*

•      MEBAC®

Finishes:

•      Mill

•      Anodized

•      Duranodic

*Only rectangular bar is serrated. I-Bar type is striated on top surface.

IB swaged aluminum  I-Bar  grating is the lightest weight, lowest cost aluminum grating. Its high strength, slip  resistant  striated  bearing  bars and  low  cost,  I-Bar  grating  is  an excellent choice when economy is a major factor.

Panel sizes:

•      3´ x 20´     2´ x 20´

•      3´ x 24´     2´ x 24´

| Weights lb./sf. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Size | Bearing Bar Depth (inches) | Swage Locked “I Bar”Type |  |  |  |  |  | Bearing Bar Dimensions (inches) | Swage Locked “Rectangular Bar”Type |  |  |  |  |  |
|  |  | IB | IF | ID | IDF | ICM4 | ICMF4 |  | BS | FS | DS | DFS | SCM4 | SCMF4 |
| 3 | - | - | - | - | - | - | - | 1” x 1/8” | 1.9 | 2.2 | 2.3 | 2.6 | 3.0 | 3.3 |
| 4 | 1” | 1.9 | 2.1 | 2.3 | 2.5 | 3.2 | 3.5 | 1” x 3/16” | 2.6 | 2.9 | 3.3 | 3.5 | 4.3 | 4.6 |
| 5 | - | - | - | - | - | - | - | 1-1/4” x 1/8” | 2.3 | 2.6 | 2.8 | 3.1 | 3.6 | 4.0 |
| 6 | 1-1/4” | 2.3 | 2.5 | 2.8 | 2.9 | 3.8 | 4.2 | 1-1/4” x 3/16” | 3.2 | 3.5 | 4.0 | 4.3 | 5.3 | 5.6 |
| 7 | - | - | - | - | - | - | - | 1-1/2” x 1/8” | 2.8 | 3.2 | 3.4 | 3.8 | 4.3 | 4.6 |
| 8 | 1-1/2” | 2.6 | 2.8 | 3.2 | 3.4 | 4.5 | 4.8 | 1-1/2” x 3/16” | 3.9 | 4.3 | 4.8 | 5.2 | 6.3 | 6.6 |
| 9 | 1-3/4” | 3.0 | 3.3 | 3.7 | 3.9 | 5.1 | 5.4 | 1-3/4” x 3/16” | 4.5 | 4.9 | 5.6 | 5.9 | 7.2 | 7.6 |
| 10 | 2” | 3.4 | 3.7 | 4.2 | 4.4 | 5.8 | 6.1 | 2” x 3/16” | 5.1 | 5.5 | 6.3 | 6.7 | 8.2 | 8.6 |
| 11 | 2-1/4” | 3.8 | 4.0 | 4.6 | 4.9 | 6.4 | 6.8 | 2-1/4” x 3/16” | 5.7 | 6.1 | 7.0 | 7.4 | 9.2 | 9.5 |
| 12 | 2-1/2” | 4.0 | 4.2 | 4.9 | 5.1 | 7.1 | 7.4 | 2-1/2” x 3/16” | 6.3 | 6.7 | 7.8 | 8.1 | 10.2 | 10.5 |

## LOAD TABLE FOR SWAGE LOCKED GRATING

This table is good for type   IB, BS, IF and FS only.

Forging partnershiSTM

| Size | 30 35 42 24 247 0.461 493 0.369 237 0.384 474 0.307 110 0.037 329 0.829 105 0.864 316 0.691 439 0.259 658 0.207 421 0.216 632 0.173 158 0.720 395 0.576 152 0.600 379 0.480 322 0.353 564 0.282 309 0.294 541 0.235 195 0.583 439 0.467 187 0.486 421 0.389 81 1.411 282 1.129 77 1.176 271 0.941 93 1.217 304 0.973 90 1.014 291 0.811 130 0.871 359 0.697 125 0.726 344 0.581 987 0.115 987 0.092 947 0.096 947 0.077 632 0.180 789 0.144 606 0.150 758 0.120 U D 1-1/4” x 3/16” or 1-1/4” I Bar 52 Span in inches 90 96 67 59 1.350 1.536 253 237 1.080 1.229 C D U D 1-1/2” x 1/8” 53 C D * Maximum span for 1/4” deflection under uniform load of 100lb/sf. Span in inches Bearing Bar Size * 35; U D C D; 355 0.191 355 0.153; 227 0.299 284 0.239; 158 0.432 237 0.345; 116 0.588 203 Span in inches 0.470 48 54 137 105 83 0.441 0.576 0.729 241 211 187 0.353 0.461 0.583 206 158 125 0.441 0.576 0.729 361 316 281 Span in inches 0.353 0.461 0.583 60 66 72 215 164 130 105 87 73 0.353 0.461 0.583 0.72 0.871 0.037 376 329 292 263 239 219 Span in inches 0.282 0.369 0.467 0.576 0.697 0.829 78 84. 3/4” x 3/16”. 1” x 1/8”; 39; U D C D; 421 0.144 421 0.115; 269 0.225 337 0.180; 187 0.324 281 0.259. 1” x 3/16” or 1” I Bar; 44; U D C D; 632 0.144 632 0.115; 404 0.225 505 0.180; 281 0.324 421 0.259. 1-1/4” x 1/8”; 47; U D C D; 658 0.115 658 0.092; 421 0.180 526 0.144; 292 0.259 439 0.207. |
| --- | --- |
| 2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 3 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 4 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 5 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 6 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 7 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 8 | 1-1/2” x 3/16” or 1-1/2” I Bar | 59 | U D C D | 1421 0.096 1421 0.077 | 909 0.150 1137 0.120 | 632 0.216 947 0.173 | 464 0.294 812 0.235 | 355 0.384 711 0.307 | 281 0.486 632 0.389 | 227 0.600 568 0.480 | 188 0.726 517 0.581 | 158 0.864 474 0.691 | 135 1.014 437 0.811 | 116 1.176 406 0.941 | 101 1.35 379 1.080 | 89 1.536 355 1.229 |
| 9 | 1-3/4” x 3/16” or 1-3/4” I Bar | 66 | U D C D | 1934 0.082 1934 0.066 | 1238 0.129 1547 0.103 | 860 0.185 1289 0.148 | 632 0.252 1105 0.202 | 484 0.329 967 0.263 | 382 0.417 860 0.333 | 309 0.514 774 0.411 | 256 0.622 703 0.498 | 215 0.741 645 0.592 | 183 0.869 595 0.695 | 158 1.008 553 0.806 | 138 1.157 516 0.926 | 121 1.317 484 1.053 |
| 10 | 2” x 3/16” or 2” I Bar | 73 | U D C D | 2526 0.072 2526 0.058 | 1617 0.113 2021 0.090 | 1123 0.162 1684 0.130 | 825 0.221 144 0.176 | 632 0.288 1263 0.230 | 499 0.365 1123 0.292 | 404 0.450 1011 0.360 | 334 0.545 919 0.436 | 281 0.648 842 0.518 | 239 0.761 777 0.608 | 206 0.882 722 0.706 | 180 1.013 674 0.810 | 158 1.152 632 0.922 |
| 11 | 2-1/4” x 3/16” or 2-1/4” I Bar | 80 | U D C D | 3197 0.064 3197 0.051 | 2046 0.100 2558 0.080 | 1421 0.144 2132 0.115 | 1044 0.196 1827 0.157 | 799 0.256 1599 0.205 | 632 0.324 1421 0.259 | 512 0.400 1279 0.320 | 423 0.484 1163 0.387 | 335 0.576 1066 0.461 | 303 0.676 984 0.541 | 261 0.784 914 0.627 | 277 0.900 853 0.720 | 200 1.024 799 0.819 |
| 12 | 2-1/2” x 3/16” or 2-1/2” I BAR | 87 | U D C D | 3947 0.058 3947 0.046 | 2526 0.090 3158 0.072 | 1754 0.130 2632 0.104 | 1289 0.176 2256 0.141 | 987 0.23 1974 0.184 | 780 0.292 1754 0.233 | 632 0.360 1579 0.288 | 522 0.436 1435 0.348 | 439 0.518 1316 0.415 | 374 0.608 1215 0.487 | 322 0.706 1128 0.564 | 281 0.810 1053 0.648 | 247 0.922 987 0.737 |

U = Uniform load lb./sf.                                                     C = Concentrated load lb./ft. of grating widht, at mid-span.                                              D = Deflection in inches.

| ALUMINUM CONVERSION FACTORS |  |  |  |  |
| --- | --- | --- | --- | --- |
| For spacings other than 1- 3/16” centers, multiply the conversion factor times the U and C values shown in the table, the D (deflection) remains as shown. |  |  |  |  |
| Type | ID / DS | IDF / DFS | ICM4 / SCM4 | ICMF4 / SCMF4 |
| Factor | 1.27 | 1.27 | 1.73 | 1.73 |

Note: The carrying capacity of a piece of grating subjected to a concentrated load over only a portion of its width is determined by the stiffness of both the bearing bars and the cross bars, and therefore differs with the type of grating used. To determine the carrying capacity of gratings subject to such loadings, the IKG engineering department should be consulted.

# Aluminum Grating

Forging partnershipsTM

Frames to fit. We offer aluminum frames for concrete embedment that are made specifically for Safe T Grid®  installation. Frames can be supplied with rubber cushion for total noise elimination and also with the same finish specified for the grating.

Comfortable. For both walking and standing. The  broad top flange walking surface feels much like solid flooring underfoot.

Will not catch high heels. Openings of Type TB-940 are less that 1/4” wide, narrower than most slender high heels, yet sufficient to allow the free passage of air and water.

Rigid, rattle-free construction. Strong, tight swaging of cross bars locks bearing bars solidly in place with a positive lock that prevents the main bearing bars from racking or “venetian blinding ”. This result will last for years without loosening even under heavy traffic. Wide top flange of bearing bars gives added lateral rigidity.

Invisible fastening system. Special clips can be supplied with the grating that lock into the bottom flange of the bearing bars. Clips can be tightened from above with a screw driver or an Allen wrench, and can just as easily be released for removing the grating to clean the collection pit.

Aluminum Grating

—.935 ——— .940

T

Depth (Size)

1-7/8”

| Size | Depth | Wt./sf. | Open Area |
| --- | --- | --- | --- |
| 4 | 1” | 2.1 | 49.9% |
| 6 | 1-1/4” | 2.8 | 49.9% |
| 8 | 1-1/2” | 3.0 | 49.9% |
| 10 | 2” | 3.4 | 49.9% |

.626

Type TB -626

H——1

| Size | Depth | Wt./sf. | Open Area |
| --- | --- | --- | --- |
| 4 | 1” | 2.7 | 47.2% |
| 6 | 1-1/4” | 3.3 | 47.2% |
| 8 | 1-1/2” | 3.6 | 47.2% |
| 10 | 2” | 4.1 | 47.2% |

.940

T

Depth (Size)

1-3/16 ”

| Size | Depth | Wt./sf. | Open Area |
| --- | --- | --- | --- |
| 4 | 1” | 3.0 | 20.8% |
| 6 | 1-1/4” | 4.2 | 20.8% |
| 8 | 1-1/2” | 4.4 | 20.8% |
| 10 | 2” | 5.0 | 20.8% |

—.311

T

Depth (Size)

15/16 ”

| Size | Depth | Wt./sf. | Open Area |
| --- | --- | --- | --- |
| 4 | 1” | 3.4 | 33.2% |
| 6 | 1-1/4” | 4.1 | 33.2% |
| 8 | 1-1/2” | 4.4 | 33.2% |
| 10 | 2” | 5.1 | 33.2% |

Type TD -626

Type TB -940

Type TP -940

3/16 ”

.626

Depth (Size)

.2475

.5615

-

Surfaces:

•      3´ x 20´      2´ x 20´

•      3´ x 24´      2´ x 24´

Panel sizes:

•      Standard striated top

•      MEBAC®

Finishes:

•      Mill

•      Anodized

•      Duranodic

## LOAD TABLE FOR SAFE T GRID®  GRATING

Forging partnershiSTM

* Maximum span for 1/4” deflection under uniform load of 100lb/sf.

| Size No. | Depth | Type | Top Flange Width | S/FT | I/FT | * 46 | U D C D | SPAN |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | 1’-0 | 1’-6 | 2’-0 | 2’-6 | 3’-0 | 3’-6 | 4’-0 | 4’-6 | 5’-0 | 5’-6 | 6’-0 | 6’-6 | 7’-0 |
| 4 | 1” | TP-940-4 | .940 | .332 | .192 |  |  | 2662 0.031 1331 0.024 | 1183 0.070 887 0.056 | 666 0.124 666 0.099 | 426 0.195 532 0.155 | 296 0.280 444 0.224 | 217 0.381 380 0.305 | 166 0.498 333 0.399 | 131 0.629 296 0.505 | 106 0.776 266 0.623 | 88 0.943 242 0.754 | 74 1.123 222 0.899 | 63 1.317 205 1.055 | 54 1.519 190 1.221 |
| 4 | 1” | TB-626-4 | .626 | .495 | .262 | 50 | U D C D | 3961 0.033 1981 0.027 | 1761 0.076 1320 0.061 | 990 0.135 990 0.108 | 634 0.212 792 0.169 | 440 0.305 660 0.244 | 323 0.415 566 0.332 | 248 0.543 495 0.434 | 196 0.688 440 0.549 | 158 0.845 396 0.678 | 131 1.026 360 0.820 | 110 1.220 330 0.976 | 94 1.436 305 1.147 | 81 1.665 283 1.330 |
| 4 | 1” | TB-940-4 | .940 | .525 | .303 | 51 | U D C D | 4204 0.031 2102 0.024 | 1868 0.070 1401 0.056 | 1051 0.124 1051 0.099 | 673 0.195 841 0.156 | 467 0.280 701 0.224 | 343 0.382 601 0.305 | 263 0.499 525 0.398 | 208 0.633 467 0.505 | 168 0.779 420 0.623 | 139 0.944 382 0.754 | 117 1.125 350 0.897 | 99 1.311 323 1.053 | 86 1.532 300 1.221 |
| 4 | 1” | TD-626-4 | .626 | .627 | .332 | 53 | U D C D | 5018 0.033 2509 0.027 | 2230 0.076 1673 0.061 | 1254 0.135 1254 0.108 | 803 0.212 1004 0.169 | 558 0.305 836 0.244 | 410 0.415 717 0.332 | 314 0.543 627 0.434 | 248 0.687 558 0.550 | 201 0.849 502 0.678 | 166 1.026 456 0.820 | 139 1.217 418 0.976 | 119 1.436 386 1.146 | 102 1.655 358 1.328 |
| 6 | 1-1/4” | TP-940-6 | .940 | .550 | .409 | 55 | U D C D | 4403 0.024 2202 0.019 | 1957 0.054 1468 0.43 | 1101 0.096 1101 0.077 | 705 0.151 881 0.120 | 489 0.217 734 0.174 | 359 0.295 629 0.237 | 275 0.386 550 0.309 | 217 0.488 489 0.391 | 176 0.604 440 0.483 | 146 0.733 400 0.584 | 122 0.868 367 0.696 | 104 1.019 339 0.818 | 90 1.187 315 0.949 |
| 6 | 1-1/4” | TB-626-6 | .626 | .757 | .505 | 58 | U D C D | 6063 0.026 3032 0.021 | 2695 0.060 2021 0.048 | 1516 0.108 1516 0.086 | 970 0.168 1213 0.135 | 674 0.243 1011 0.194 | 495 0.330 866 0.264 | 379 0.432 758 0.345 | 299 0.545 674 0.437 | 243 0.676 606 0.539 | 200 0.814 551 0.653 | 168 0.969 505 0.777 | 144 1.144 466 0.911 | 124 1.325 433 1.058 |
| 6 | 1-1/4” | TB-940-6 | .940 | .869 | .646 | 62 | U D C D | 6952 0.024 3476 0.019 | 3090 0.054 2317 0.043 | 1738 0.096 1738 0.077 | 1112 0.151 1390 0.120 | 772 0.217 1159 0.174 | 568 0.296 993 0.236 | 435 0.387 869 0.309 | 343 0.489 772 0.391 | 278 0.604 695 0.483 | 230 0.732 632 0.585 | 193 0.870 579 0.696 | 165 1.024 535 0.817 | 142 1.186 497 0.948 |
| 6 | 1-1/4” | TD-626-6 | .626 | .960 | .640 | 62 | U D C D | 7680 0.027 3840 0.021 | 3413 0.060 2560 0.048 | 1920 0.108 1920 0.086 | 1229 0.168 1536 0.135 | 853 0.242 1280 0.194 | 627 0.330 1097 0.264 | 480 0.432 960 0.345 | 379 0.546 853 0.437 | 307 0.674 768 0.54 | 254 0.817 698 0.653 | 213 0.970 640 0.777 | 182 1.142 591 0.912 | 157 1.325 549 1.059 |
| 8 | 1-1/2” | TP-940-8 | .940 | .742 | .652 | 62 | U D C D | 5939 0.020 2970 0.016 | 2640 0.046 1980 0.036 | 1485 0.081 1485 0.065 | 950 0.127 1188 0.102 | 660 0.184 990 0.147 | 485 0.250 848 0.200 | 371 0.327 742 0.261 | 293 0.414 660 0.331 | 238 0.512 594 0.409 | 196 0.618 540 0.495 | 165 0.737 495 0.589 | 141 0.867 457 0.692 | 121 1.001 424 0.802 |
| 8 | 1-1/2” | TB-626-8 | .626 | 1.010 | .798 | 65 | U D C D | 8084 0.022 4042 0.018 | 3593 0.051 2695 0.041 | 2021 0.091 2021 0.072 | 1293 0.142 1617 0.113 | 898 0.205 1347 0.164 | 660 0.279 1155 0.223 | 505 0.364 1011 0.291 | 399 0.461 898 0.369 | 323 0.568 808 0.455 | 267 0.688 735 0.551 | 225 0.821 674 0.656 | 191 0.960 622 0.770 | 165 1.116 577 0.892 |
| 8 | 1-1/2” | TB-940-8 | .940 | 1.172 | 1.030 | 70 | U D C D | 9378 0.020 4689 0.016 | 4168 0.046 3126 0.036 | 2344 0.081 2344 0.065 | 1500 0.127 1876 0.102 | 1042 0.184 1563 0.147 | 766 0.250 1340 0.200 | 586 0.327 1172 0.261 | 463 0.414 1042 0.331 | 375 0.511 938 0.409 | 310 0.619 853 0.495 | 260 0.735 781 0.589 | 222 0.865 721 0.691 | 191 1.001 670 0.802 |
| 8 | 1-1/2” | TD-626-8 | .626 | 1.280 | 1.011 | 69 | U D C D | 10240 0.022 5120 0.018 | 4551 0.051 3413 0.041 | 2560 0.091 2560 0.072 | 1638 0.142 2048 0.113 | 1138 0.205 1707 0.164 | 836 0.279 1463 0.223 | 640 0.364 1280 0.291 | 506 0.461 1138 0.369 | 410 0.570 1024 0.445 | 339 0.690 931 0.511 | 284 0.818 853 0.655 | 242 0.961 788 0.770 | 209 1.116 731 0.892 |
| 10 | 2” | TP-940-10 | .940 | 1.177 | 1.350 | 75 | U D C D | 9421 0.015 4710 0.012 | 4187 0.035 3140 0.028 | 2355 0.062 2355 0.050 | 1507 0.098 1884 0.078 | 1047 0.141 1570 0.113 | 769 0.192 1346 0.153 | 589 0.251 1178 0.200 | 465 0.317 1047 0.254 | 377 0.392 942 0.313 | 311 0.474 856 0.379 | 262 0.565 785 0.452 | 223 0.663 725 0.530 | 192 0.768 673 0.615 |
| 10 | 2” | TB-626-10 | .626 | 1.586 | 1.647 | 78 | U D C D | 12692 0.017 6346 0.013 | 5641 0.039 4231 0.031 | 3173 0.069 3173 0.055 | 2031 0.108 2538 0.086 | 1410 0.156 2115 0.124 | 1036 0.212 1813 0.169 | 793 0.277 1587 0.221 | 627 0.351 1410 0.280 | 508 0.433 1269 0.346 | 420 0.524 1154 0.419 | 353 0.624 1058 0.499 | 300 0.731 976 0.585 | 259 0.849 907 0.679 |
| 10 | 2” | TB-940-10 | .940 | 1.859 | 2.132 | 84 | U D C D | 14875 0.015 7438 0.012 | 6611 0.035 4958 0.028 | 3719 0.062 3719 0.050 | 2380 0.098 2975 0.078 | 1653 0.141 2479 0.113 | 1214 0.192 2125 0.153 | 930 0.251 1859 0.200 | 735 0.318 1653 0.254 | 595 0.392 1488 0.314 | 492 0.475 1352 0.379 | 413 0.564 1240 0.452 | 352 0.663 1144 0.530 | 304 0.770 1063 0.615 |
| 10 | 2” | TD-626-10 | .626 | 2.009 | 2.086 | 83 | U D C D | 16077 0.017 8038 0.013 | 7145 0.039 5359 0.031 | 4019 0.069 4019 0.055 | 2572 0.108 3215 0.086 | 1786 0.156 2679 0.124 | 1312 0.212 2297 0.169 | 1005 0.277 2010 0.221 | 794 0.351 1786 0.280 | 643 0.433 1608 0.346 | 531 0.523 1462 0.419 | 447 0.624 1340 0.499 | 381 0.733 1237 0.586 | 328 0.849 1148 0.679 |

U = Uniform load lb./sf.                                                    C = Concentrated load, lb./ft. of grating width, at mid-span.                                        D = Deflection in inches.

Theoretical values based on f = 12,000 PSI, E = 10,000,000 psi, gross section of bearing bar.

Note: All deflections are theoretical and are based on standard engineering practices. They are provided for design selection only and should not be considered as absolute.

# Pressure Locked Grating

1- 3/16“

1- 3/16“

Type

B

F

D

DF

|  | 4 ” |  |
| --- | --- | --- |

SPAN

|  |  |  | 2” |
| --- | --- | --- | --- |

SPAN

t             4 ”          s

15/16“

SPAN

- 2”

15/16“  	 SPAN

Forging partnershipsTM

Recommended for  general applications.

Closer cross bars. Best   for heavy public traffic, or where smaller openings are required.

Same as type B but closer bearing bars for conditions where more steel area is  required.

With closer cross bar and bearing bars. For conditions requiring greatly reduced net opening.

Pressure Locked Grating

Pressure locked grating incorporates tight-fitting, slotted bearing bars and cross bars, locked together. The permanent locking of the bars is accomplished by slotting the bearing bars with a wider “dovetail” shape at the bottom of the slot.

The bearing bar slot is usually 1/2 the depth of the cross bar. The cross bars are slotted to a depth slightly less than half the bar depth. When the bars are press together under hydraulic pressure, the cross bar material is forced into the “dovetail” shape of the bearing bar notch, forming a strong, rigid unit.

| Weights lb./sf. |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Bar Size | Bearing Bar Dimensions (inches) | STEEL |  |  |  | ALUMINUM |  |  |  |
|  |  | B | D | F | DF | B | D | F | DF |
| 1 | 3/4” x 1/8” | 4.4 | 4.8 | 4.6 | 5.5 | 1.6 | 1.7 | 1.7 | 2.0 |
| 2 | 3/4” x 3/16” | 5.7 | 7.0 | 6.4 | 7.7 | 2.0 | 2.5 | 2.2 | 2.7 |
| 3 | 1” x 1/8” | 5.2 | 6.4 | 6.0 | 7.2 | 1.9 | 2.3 | 2.2 | 2.6 |
| 4 | h | 7.5 | 9.3 | 8.3 | 10.1 | 2.6 | 3.3 | 2.9 | 3.5 |
| 5 | 1-1/4” x 1/8” | 6.3 | 7.9 | 7.1 | 8.7 | 2.3 | 2.8 | 2.6 | 3.1 |
| 6 | 1-1/4” x 3/16” | 9.1 | 11.3 | 9.9 | 12.2 | 3.2 | 4.0 | 3.5 | 4.3 |
| 7 | 1-1/2” x 1/8” | 7.6 | 9.5 | 8.7 | 10.6 | 2.8 | 3.4 | 3.2 | 3.8 |
| 8 | 1-1/2” x 3/16” | 11.0 | 13.7 | 12.1 | 14.8 | 3.9 | 4.8 | 4.3 | 5.2 |
| 9 | 1-3/4” x 3/16” | 12.7 | 15.8 | 13.8 | 16.9 | 4.5 | 5.6 | 4.9 | 5.9 |
| 10 | 2” x 3/16” | 14.3 | 17.9 | 15.4 | 19.0 | 5.1 | 6.3 | 5.5 | 6.7 |
| 11 | 2-1/4” x 3/16” | 16.0 | 20.0 | 17.1 | 21.1 | 5.7 | 7.0 | 6.1 | 7.4 |
| 12 | 2-1/2” x 3/16” | 17.7 | 22.1 | 18.8 | 23.2 | 6.3 | 7.8 | 6.7 | 8.1 |

Installation note:

Pressure locked grating should be installed with the “flush” side up. On 3/4 deep pressure locked grating where the cross bars and bearing bars are the same depth. IKG will mark the grating showing the top side for installation.

Top side

Flush cross bar

| Surfaces: • Plain • Serrated • MEBAC® Finishes: • Mill • Galvanized • Painted | Panel sizes: • 3´ x 12´ • 2´ x 12´ Available in: • Carbon Steel • Stainless Steel (304L & 316L) • Aluminum |
| --- | --- |

# Pressure Locked Close Mesh

Forging partnershiSTM

High heel proof 1/4” Clear opening.

Pressure locked grating is available with these close bar spacing to accommodate requirements for pedestrian comfort and safety as well as many other architectural needs for special grating for a particular job.

| Weights lb./sf. |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Bar Size | Bearing Bar Dimensions (inches) | STEEL |  |  |  |  | ALUMINUM |  |  |  |  |
|  |  | CM-1 | CM-2 | CM-3 | CM-4 | CM-5 | CM-1 | CM-2 | CM-3 | CM-4 | CM-5 |
| 1 | 3/4” X 1/8” | - | 8.6 | 6.9 | - | 5.5 | - | 3.1 | 2.4 | - | - |
| 2 | 3/4” X 3/16” | 13.7 | 13.3 | - | 9.0 | 7.8 | 4.7 | 4.1 | - | 3.1 | 2.7 |
| 3 | 1” X 1/8” | - | 11.5 | 9.0 | - | 7.1 | - | 4.2 | 3.1 | - | - |
| 4 | 1” X 3/16” | 18.1 | 16.5 | - | 11.9 | 10.2 | 6.2 | 5.5 | - | 4.1 | 3.5 |
| 5 | 1-1/4” X 1/8” | - | 14.2 | 11.2 | - | 8.9 | - | 5.2 | 3.9 | - | - |
| 6 | 1-1/4” X 3/16” | 22.6 | 20.7 | - | 14.8 | 12.7 | 7.8 | 6.9 | - | 5.1 | 4.4 |
| 7 | 1-1/2” X 1/8” | - | 17.2 | 13.5 | - | 10.8 | - | 6.3 | 4.7 | - | - |
| 8 | 1-1/2” X 3/16” | 27.2 | 25 | - | 17.8 | 15.3 | 9.4 | 8.3 | - | 6.2 | 5.3 |
| 9 | 1-3/4” X 3/16” | 31.6 | 29.4 | - | 20.8 | 17.8 | 10.9 | 9.6 | - | 7.2 | 6.1 |
| 10 | 2” X 3/16” | 36.2 | 33.2 | - | 23.8 | 20.5 | 12.5 | 11.0 | - | 8.2 | 7.1 |
| 11 | 2-1/4” X 3/16” | 40.1 | 37.3 | - | 26.5 | 22.7 | 14 | 12.4 | - | 9.1 | 7.8 |
| 12 | 2-1/2” X 3/16” | - | 41.4 | - | 29.5 | 25.0 | - | 14.8 | - | 10.0 | 8.6 |

Type

CM1

CM2

CM3

CM4

CM5

| 7/16“: 1/2“ 5/8 “ | 4”. SPAN 4”. SPAN 4”. SPAN |  |
| --- | --- | --- |

|  | 4” |  |
| --- | --- | --- |

11/16 “:

SPAN

|  | 4” |  |
| --- | --- | --- |

13/16 “

SPAN

Our closest spaced grating available. Excellent for

pedestrian use and areas

where high visibility is a

concern. Satisfies maximum 1/2” clear opening as

required by ADA.

Same as CM 1 only with a slightly increased opening. Satisfies maximum 1/2” clear opening as required by ADA.

As with the other close mesh types, this style resists all small objects from falling through. Satisfies maximum 1/2”clear opening as required by ADA.

Provides larger open area for use where more ventila- tion is required beneath the grating. Satisfies, maximum 1/2” clear opening as required by ADA.

Recommended for general applications.

Visit our website for loading information.

ADA  Compliance:

If gratings are located in walking surfaces, then they shall have spaces no greater than ½ inch wide in one direction. If gratings have elongated openings, then they shall be placed so that the long dimension is perpendicular to the dominant direction of travel.

Flush cross bar

| Surfaces: • Plain • Serrated • MEBAC® Finishes: • Mill • Galvanized • Painted • GrateCoat® | Panel sizes: • 3´ x 12´ • 2´ x 12´ Available in: • Carbon Steel • Stainless Steel (304L & 316L) • Aluminum |
| --- | --- |

# Treads

Nosing Types

1-1/4”

Checkered Plate

Steel Treads

only.

Integral MEBAC®

Angle Nosing

1-1/4” Cast

Aluminum Abrasive

Steel and Aluminum

Treads

1-1/4” Corrugated Aluminum Extruded

Aluminum Tread only.

Forging partnershipsTM

IKG recommends the treads for stairs where maximum safety is required.

| Grating Type Available: • Weldforged® • Swage Locked • Pressure Locked • Riveted Surfaces: • Plain • Serrated • MEBAC® | Finishes: • Mill • Galvanized • Painted • GrateCoat® Material Available: • Carbon Steel • Stainless Steel (304L & 316L) • Aluminum |
| --- | --- |

ha “ o holes in stringer RUN RISE 1/2 ” min. Top of platform or finished floor RISE tread WIDTH

Note: Tread width should always be greater than tread run by 1/2 in. (12mm) minimum.

Carrier Plate

B

C

+

(See page 12) Finished Depth

| Dimension B • Steel Treads 1-3/4” up to including 1-1/4 ” deep treads. 2-1/4 ” for others | Dimension B • Aluminum treads through 1-3/4” bearing bar depth will be 2-1/4” |
| --- | --- |

7/16” Ø hole & slot, for 3/8 ” Ø bolt

Note: Bolts for mounting to stringers not supplied.

# Treads

| Table of Standard Tread Depths for: |  |  |  |
| --- | --- | --- | --- |
| Pressure Locked | Swage Locked | Riveted | *(Dimension A) Hole Centers |
| Welded |  |  |  |
| B; W/B | IB | Type K (3/16 B.B.) |  |
| 6-3/16“ | 6-1/4“ | 6-11/16“ | 2-1/2“ |
| 7-3/8“ | 7-7/16“ | 8“ | 4-1/2“ |
| 8-9/16“ | 8-5/8“ | 9-5/16“ | 4-1/2“ |
| 9-3/4“ | 9-13/16“ | 10-5/8“ | 7“ |
| 10-15/16“ | 11“ | 11-15/16“ | 7“ |
| 12-1/8“ | 12-3/16“ | 13-1/4“ | 7“ |

| DIMENSION B in TREAD with carrier plate detail in. (mm) |  |
| --- | --- |
| Grating Depth | *Dimension B |
| 3/4“ to 1/4“ 1-1/2“and up | 1-3/4“ 2-1/4“ |
| Aluminum is usually 2-1/4 | ” (57) regardless of depth |

*See Page 11

Forging partnershiSTM

*Maximum   tread   length based on 300  lb  (133  kN) concentrated load on front

5 in. (127 mm) of tread at center of tread length and deflection limitation of L/240 of   length.   For   maximum length under other loadings, consult the manufacturer.

Recommended Bearing Bar Sizes

| SteelTreads |  |  |  |  |
| --- | --- | --- | --- | --- |
| Bearing Bar Size in. (mm) 3/4” x 3/16” | MaximumTread Length* |  |  |  |
|  | @ 1-3/16” (30) o.c. |  | @ 15/16” (24) o.c. |  |
|  | Plain 2´- 4” | Serrated - | Plain 2´- 8” | Serrated - |
| 1” x 3/16” | 3´- 5” | 2´- 10” | 4´- 0” | 3´- 4” |
| 1-1/4” x 3/16” | 4´- 8” | 4´- 2” | 5´- 1” | 4´- 6” |
| 1-1/2” x 3/16” | 5´- 6” | 5´- 3” | 5´- 6” | 5´- 6” |

| Aluminum Treads (Rectangular Bars) |  |  |  |  |
| --- | --- | --- | --- | --- |
| Bearing Bar Size in. (mm) 1” x 3/16” | MaximumTread Length* |  |  |  |
|  | @ 1-3/16” (30) o.c. |  | @ 15/16” (24) o.c. |  |
|  | Plain 2´- 4” | Serrated - | Plain 2´- 6” | Serrated - |
| 1-1/4” x 3/16” | 2´- 10” | 2´- 7” | 3´- 1” | 2´- 9” |
| 1-1/2” x 3/16” | 3´- 6” | 3´- 2” | 3´- 10” | 3´- 6” |
| 1-3/4” x 3/16” | 4´- 3” | 3´- 10” | 4´- 8” | 4´- 3” |

| Aluminum Treads I Bars |  |  |
| --- | --- | --- |
| Bearing Bar Size in. (mm) 1” I | MaximumTread Length* |  |
|  | @ 1-3/16” (30)o.c. 2´- 4” | @ 15/16” (24)o.c. 2´- 6” |
| 1-1/4” I | 2´- 10” | 3´- 1” |
| 1-1/2” I | 3´- 6” | 3´- 10” |
| 1-3/4” I | 4´- 3” | 4´- 8” |

| Safe T Grid® Treads Recommended Spans |  |  |
| --- | --- | --- |
| Size | General Pu blic Use | Commercial / Industrial |
| 1”TP - 940 | 2´- 2 | 2´- 2 |
| 1”TB - 626 | 2´- 4 | 2´- 7 |
| 1”TB - 940 | 2´- 5 | 2´- 9 |
| 1”TD - 626 | 2´- 6 | 2´- 11 |
| 1-1/4”TP - 940 | 2´- 11 | 3´- 3 |
| 1-1/4”TB - 626 | 2´- 11 | 3´- 5 |
| 1-1/4”TB - 940 | 3´- 3 | 3´- 9 |
| 1-1/4”TD - 626 | 3´- 3 | 3´- 9 |
| 1-1/2”TP - 940 | 3´- 6 | 4´- 1 |
| 1-1/2”TB - 626 | 3´- 7 | 4´- 2 |
| 1-1/2”TB - 940 | 4´- 0 | 4´- 7 |
| 1-1/2”TD - 626 | 3´- 11 | 4´- 7 |
| 2”TP - 940 | 4´- 10 | 5´- 7 |
| 2”TB - 626 | 4´- 11 | 5´- 8 |
| 2”TB - 940 | 5´- 4 | 6´- 2 |
| 2”TD - 626 | 5´- 4 | 6´- 1 |

1. Recommended span for general uses for Safe T Grid®   is developed by using a concentrated load of 300 pound with a 33%  impact at midspan supported by:

Nosing plus 3 “T” bars forTP spacing

Nosing plus 4 “T” bars forTB spacing

Nosing plus 5 “T” bars for TD spacing

with a deflection not to exceed L/240 or .250 inches.

2. Recommended span for commercial / industrial uses is developed by using the same loading criteria as for general public but with a deflection not to exceed L/180 or .375 inches.

Type

HWB

HWD

HWC

HWP

HWL

4”

1- 3/   “

16

SPAN

—— 4”

15/16 “

SPAN

4”

1- 3/8 “

SPAN

4 ”

1- 7/8“

4 ” 2- 3/8 “

Heavy Duty Grating

Forging partnershipsTM

Bearing bars 1-3/16“ c/c Cross Bars 4” c/c

Bearing bars 15/16“ c/c Cross Bars 4” c/c

Bearing bars 1-3/8 “ c/c Cross Bars 4” c/c

Bearing bars 1-7/8 “ c/c Cross Bars 4” c/c

Bearing bars 2-3/8“ c/c Cross Bars 4” c/c

Product designation

For Drains, Trenches and Scuppers.

Design criteria

Style:

EC: Welded construction with rectangular cross bar welded at each joint.

HW: Welded construction with round cross bars welded at each joint.

Basis of Design for Heavy Duty Grating

Bar SizeThickness:

Bar Size Designation:

A = 1/4” B = 5/16” C = 3/8”

Size # 10 = 2”

Size # 12 = 2-1/2”

Size # 14 = 3”

Size # 16 = 3-1/2”

Size # 18 = 4”

AASHTO (American Association Society of State Highway Transportation Officials) Loadings for H-10, H-15, H-20

| Wheel Load | H-10 | 10,400 Ibs. | (10”X10” print) |
| --- | --- | --- | --- |
|  | H-15 | 15,600 Ibs. | (15”X15” print) |
|  | H-20 | 20,800 Ibs. | (20”X20” print) |

•      Impact Factor, 30%

•      Method of Load Distribution:

Each wheel distributed over a width of 10” (H-10); 15”

EXAMPLE: A product that has a main bar of 3-1/2” X 1/4” with the main bars spaced 1-3/8” o.c. is designated: HWC16A

(H-15); 20” (H-20) plus 2 times the distance center-to- center of the bearing bars over a length on each bar equal to 10” for H-10, 15” for H-15 and 20” for H-20.

•      Maximum allowable stress in accordance with AASHTO specifi- cations for highway bridges, 1984 edition.

•      Simple span.

All Heavy Duty Grating subject to rolling loads will be load banded, regardless of span.

| Size of Bearing Bar 2” X 1/4” | Type / Style / Size C10A | Weights lb./sf. |  | Type / Style / Size P10A | Weights lb./sf. |  | Type / Style / Size L10A | Weights lb./sf. |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | EC 16.46 | HW 16.42 |  | EC 13.12 | HW 13.02 |  | EC 10.62 | HW 10.47 |
| 2” X 3/8” | C10C | 24.32 | 24.95 | P10C | 19.34 | 19.85 | L10C | 15.61 | 16.03 |
| 2-1/2” X 1/4” | C12A | 20.68 | 20.25 | P12A | 16.51 | 16.00 | L12A | 13.38 | 12.81 |
| 2-1/2” X 3/8” | C12C | 30.52 | 30.69 | P12C | 24.31 | 24.32 | L12C | 19.64 | 19.53 |
| 3” X 1/4” | C14A | 24.86 | 24.08 | P14A | 18.97 | 18.19 | L14A | 15.56 | 14.78 |
| 3” X 3/8” | C14C | 36.9 | 36.36 | P14C | 28.08 | 27.54 | L14C | 22.98 | 22.44 |
| 3-1/2” X 1/4” | C16A | 28.73 | 27.95 | P16A | 21.85 | 21.07 | L16A | 17.86 | 17.08 |
| 3-1/2” X 3/8” | C16C | 42.55 | 42.01 | P16C | 32.28 | 31.74 | L16C | 26.34 | 25.8 |
| 4” X 1/4” | C18A | 34.44 | 31.19 | P18A | 26.59 | 23.88 | L18A | 22.04 | 19.33 |
| 4” X 3/8” | C18C | 49.58 | 47.754 | P18C | 37.84 | 36.01 | L18C | 31.04 | 29.22 |

Please call for vehicular traffic table, panel sizes and spacing for increased lateral stability due to turning traffic and traffic traveling perpendicular to span.

# Railroad Grating

| AAR Group # | Size of Bearing Bar | IKG Symbol | Weight Per Sq. Ft. | Unsupported Span not to excced |
| --- | --- | --- | --- | --- |
| 1 | 1” x 1/8” | WRR3BC | 3.18 | 4 ' 0” |
| 2 | 1-1/2“ x 3/16” | WRR8 | 8.33 | 7 ' 0” |
| 3 | 2” x 3/16” | WRR10 | 10.55 | 10 ' 0” |

| Group # 1 WRR3BC 1.583” c/c | Group # 2 & 3 WRR8 WRR10 1.643” c/c | No. Bars |
| --- | --- | --- |
| 1-11/16” | 1-13/16” | 2 |
| 3-9/32” | 3-15/32” | 3 |
| 4-7/8” | 5 -1/8” | 4 |
| 6-15/32” | 6 -3/4” | 5 |
| 8-1/32” | 8 -13/32” | 6 |
| 9-5/8” | 10 -1/16” | 7 |
| 11-7/32” | 11-11/16” | 8 |
| 1' 0-25/32” | 1' 1- 3/16” | 9 |
| 1' 2- 3/8” | 1' 2- 31/32” | 10 |
| 1' 3-31/32” | 1' 4-5/8” | 11 |
| 1' 5-17/32” | 1' 6 -1/4” | 12 |
| 1' 7-1/8” | 1' 7-7/8” | 13 |
| 1' 8-23/32” | 1' 9-17/32” | 14 |
| 1' 10-9/32” | 1' 11- 3/16” | 15 |
| 1' 11-7/8” | 2' 0 -13/16” | 16 |
| 2' 1-7/16” | 2' 2-1/2” | 17 |
| 2' 3” | 2' 4-1/8” | 18 |
| 2' 4-5/8” | 2' 5 -3/4” | 19 |
| 2' 6-3/16” | 2' 7-13/32” | 20 |
| 2' 7-25/32” | 2' 9 -1/16” | 21 |
| 2' 9-3/8” | 2' 10 -11/16” | 22 |
| 2' 10 -15/16” | 3' 0-11/32” | 23 |
| 3' 0-17/32” | 3' 1-31/32” | 24 |

Forging partnershiSTM

WRR - BC

WRR -TC

4”

1.583 “

4”

1.643 “

Type

Rectangular bearing bar

Twisted square cross bar

Weldforged® joints

Approved by:

•  Association of American Railroads (AAR).

Produced in two bar spacings

•   Box Car

1.583” ctr. - ctr. Bearing Bars • Tank Car

1.643” ctr. - ctr. Bearing Bars

Produced in two bar thicknesses

•  1/8” thick

• 3/16” thick

Weldforged® construction

• for durability

Carbon Steel

• for strength

Serrated top surface

• for slip resistance

# Riveted Grating

| Weights lb./sf. |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Bar Size | Bearing Bar Dimensions (inches) | STEEL |  |  |  |  | ALUMINUM |  |  |  |  |
|  |  | K | J | U | UJ | W | K | J | U | UJ | W |
| 1 | 3/4” x 1/8” | 6.5 | 9.0 | 7.0 | 7.9 | 4.9 | 2.3 | 3.3 | 2.4 | 2.7 | 1.7 |
| 2 | 3/4” x 3/16 | 8.0 | 10.4 | 8.5 | 9.7 | 5.9 | 2.8 | 3.8 | 2.9 | 3.3 | 2.0 |
| 3 | 1” x 3/8” | 7.5 | 10.5 | 8.0 | 11.1 | 5.7 | 2.7 | 3.8 | 2.7 | 3.8 | 2.0 |
| 4 | 1” x 3/16” | 9.0 | 12.5 | 9.5 | 13.2 | 7.0 | 3.3 | 4.5 | 3.2 | 4.5 | 2.4 |
| 5 | 1-1/4” x 1/8” | 8.5 | 12.0 | 9.0 | 12.6 | 6.5 | 3.1 | 4.3 | 3.1 | 4.3 | 2.3 |
| 6 | 1-1/4” x 3/16” | 10.5 | 14.7 | 11.0 | 15.3 | 8.1 | 3.8 | 5.3 | 3.8 | 5.2 | 2.8 |
| 7 | 1-1/2” x 1/8” | 9.5 | 13.5 | 10.0 | 14.2 | 7.3 | 3.5 | 4.9 | 3.4 | 4.9 | 2.5 |
| 8 | 1-1/2” x 3/16” | 12.0 | 16.8 | 12.5 | 17.4 | 9.2 | 4.4 | 6.0 | 4.3 | 6.0 | 3.2 |
| 9 | 1-3/4” x 3/16” | 13.5 | 18.8 | 14.0 | 19.4 | 10.4 | 4.9 | 6.8 | 4.8 | 6.7 | 3.6 |
| 10 | 2” x 3/16” | 16.0 | 22.9 | 17.0 | 23.3 | 12.3 | 5.8 | 8.0 | 5.8 | 8.0 | 4.2 |
| 11 | 2-1/4” x 3/16” | 17.5 | 25.0 | 18.5 | 25.4 | 13.3 | 6.4 | 8.8 | 6.4 | 8.7 | 4.6 |
| 12 | 2-1/2” x 3/16” | 19.0 | 27.1 | 20.0 | 27.8 | 14.4 | 7.0 | 9.6 | 7.2 | 9.7 | 5.0 |

Forging partnershipsTM

Type

K

J

U

UJ

W

7”

## 1” CLEAR OPENING

SPAN

t                 7”

<>.一

5/8”CLEAR OPENING

SPAN

— 3- 1/2 ”一

w      w

!

## 1” CLEAR OPENING

SPAN

|  | 3- 1/2 ” |  |
| --- | --- | --- |

5/8”CLEAR OPENING

SPAN

<                                               7”

-/2”CLEAR OPENING

SPAN

Recommended for general applications.

Ornamental design with close bar

centers. Excellent for pedestrian traffic.

Ornamental design

with closer bar centers. Easy under foot.

Combines the closer bar and rivet centers of the U and J.

Economical type

for special industrial uses where wider

opening can be used.

Available in:

•      Carbon Steel

•      Stainless Steel (304L & 316L)

•      Aluminum

Surfaces:

•      Plain

•      Serrated

Finishes:

•      Mill

•      Galvanized

•      GrateCoat®

Please call for load information and panel sizes.

# Surfaces and

# Finishes

Forging partnershiSTM

SURFACES

Plain (smooth)

Top surface is available for all products: steel, stain- less steel and aluminum grating products.

Serrated (slip resistant)

Top surface for all products, except Aluminum I-Bar, Flush Top, and Safe T Grid® . Serrated offers more secure footing, where oil, water or chemicals are present.

MEBAC® (Metal Bonded Anti-Slip Coatings)

MEBAC  products  are   manufactured  using  abrasive grit particles encapsulated in metal spray arc that is bonded to an aluminum or steel substrate. MEBAC offers  a  consistently  high  coefficient  of  friction under a wide range of conditions, even when wet with lubricants such as brake fluid and oil, providing margins of safety that are unmatched in the industry. Visit: www.MEBAC.com

FINISHES

Mill. For carbon steel grating, refers to the natural finish of carbon steel as it comes from the mill. Mill Finish is our standard stainless steel and aluminum grating finish. The welded stainless steel grating and the aluminum grating undergoes  caustic  cleaning after  fabrication  which causes discoloration of the finished product.

Galvanized. A galvanized steel finish is the best protection for corrosion resistance for steel grating because the zinc metallurgically bonds with to the steel, creating a series of highly corrosion-resistant zinc-iron alloy layers. IKG’s galvanized steel is galva- nized per ASTM A-123 industry standard.

GrateCoat® . IKG offers the highest quality standard paint finish in the Industry. GrateCoat®  powder coat finish.

•      Standard Steel of 1/8 ” and 3/16 ” conforms to ASTM A1011 CS type B.

•      Wire Cross Rods for Welded Grating conform to ASTM A510.

•      Steel Bars of 1/4 ” and heavier conforms to ASTM A36.

•      Aluminum bars and extrusions conform to ASTM B221 alloy 6063-T6 for bearing  bars and 6060-T1 for cross bars.

•      Stainless Steel material conforms to ASTM A167 type 304L or type 316L.

Anodized. Oxide coatings of different colors and hard, wear-resisting surface finishes can be applied in aluminum grating.

## MATERIALS

# Fastening Methods

Forging partnershipsTM

SADDLE CLIP:

A special bent-clip type bar grating fastener for removable bar grating panels available in aluminum, stainless steel, and galvanized steel. Cross bars may need to be snipped in the field to facilitate placement of saddle clips.

PLATE FASTENERS (aka LUGS/ANCHOR BLOCKS)

Plate fasteners of 1⁄4” or 3⁄16” thick aluminum or steel may be shop welded by the grating manufacturer and used to fasten permanent or removable grating panels. Plate fasteners are recessed thus offering a trip-free surface.

G-CLIP:

Available in aluminum, stainless steel, and galvanized steel used in conjunction with bar grating and embedded grating frames. Cross bars may need to be snipped in the field to facilitate placement of bar grating clamps.

Z CLIP:

Especially helpful in holding down riveted grating. Z Clips are manufactured from stainless steel and are available in 1” (1” and 1-1/4” grating) 1-1/2” (1-1/2” and 1-3/4” grating) and 2” (2”, 2-1/4” and 2-1/2” grating) with a pre-punched hole to accept a 1/4” bolt or TEK screw (by others).

HILTI DISK:

For a wide range of grating fastening applications like: oil and gas installations, offshore and ship building, industrial construction, steel industry, other public facilities, among others.

COUNTERSUNK LAND:

For close-mesh aluminum grating (7/16” bearing bar centers) a countersunk land may be drilled by the grating manufacturer for use with a 1/4” diameter TEK screw (by others).

WELD INSTALLATION:

Tack weld the third bearing bar from each panel side to the support member with 3/16” fillet welds x 3/4” long, plus weld in center of panel at intermediate supports when appropriate.

# Engineering Data

Forging partnershiSTM

INSTALLATION CLEARANCE

GLOSSARY OF TERMS

SPAN CRS. OF SUPPORTS

LENG (SPAN) TH

WIDTH

BEARING BAR (Load Bar)

Uniform  Load  carrying  bar  spanning across supporting members.

CROSS BAR (Twisted)

Uniform  rod,  in  square  twisted  steel, forged into and at right angles to the load bar.

BANDING BAR (Edge Bar)

Trim  bar,  generally  as  same  size  as load bars, welded to ends of load bars across panel ends and around notches and penetrations (if any).

LENGTH OF PANEL (Span)

Overall dimension of a panel measured parallel  with  load  bars.  (Indicated  by   symbol)

WIDTH OF PANEL

Overall dimension of a panel measured at right angles to the load bars. (Always called “width” even if greater than the length.)

SERRATIONS

Small notches made in the top edge of the load bar to assist in skid resistance.

NOSING

A member attached to or on the leading edge of a stair tread to assist in skid resistance.

KICK PLATE (Toe Plate)

Heavy section flat bar welded to ends or sides of panels and around cut-outs, etc., when specified. Top edge to be 4” above grating generally.

CUT OUTS

Grating  areas  removed  from  panel  to permit passage or installation of pipes, equipment,    structural    and    handrail items.

1/4 ”

1/4 ”

Nominal

Panel Width      Panel Width

Panel Span                           Panel Span

| 3/8 ” |  |  |  |  |  | Nominal |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |

1/4 ”

Actual Cutout will be to nearest load bar

3/8 ”

〈             Nominal

Load Bar (typical)

1/4 ”

|  | 1/4 ” |
| --- | --- |

Min. clearance equal to embed angle thickness NOTE Clearance can vary relative to embed angle straightness.

1/2 ”

Manufacturing Facilities

Division Headquarters

1514 South Sheldon Road Houston, TX 77015

P. O. Box 310

Channelview, TX 77530 Phone: (281) 452-6637 Fax: (281) 457-6054

Garrett, IN.

1801 Forrest Park Drive Garrett, IN 46738

Phone: (260) 357-6900

Fax: (260) 357-0027

## Leeds, Al.

8500 Dunnavant Road Leeds, AL 35094

Phone: (205) 699-2111

Fax: (205) 699-8388

## Reno, NV.

6645 Echo Ave Suite C Reno, NV 89506

Phone: (713) 378-3935

Sand Springs, OK.

920 East Pecan

Sand Springs, OK 74063 Phone: (918) 246-0772

Fax: (918) 246-0783

Querétaro, México.

Rejillas Irving

Prol. Corregidora Nte. 487 Col. Parques Industriales Querétaro, Qro. 76160

Phone: 52 (442) 227-1000

Fax: 52 (442) 227-1001

www.IKG.com

Call us at (800) 324-8417

IKG

Forging partnershiSTM

NAAMM

National Association of

Architectural Metal Manufacturers

MEMBER

© 2020 IKG USA, LLCAll rights reserved. 03-2020 (250)